A

Major project

On

“Analysis of Si-Mo S.G. IRON manufacturing techniques & the effects of heat treatment on its microstructure USING  IMAGE analysis technique”

Submitted in Partial Fulfilment of the requirement

for the award of degree of

MASTER OF ENGINEERING

in

PRODUCTION ENGINEERING

By

Rishi Kant

(Univ. Roll No.-2404)

Under the Guidance of

Shri. VIJAY GAUTAM

(Senior Lecturer)

Department of Mechanical and Production Engineering

Delhi College of Engineering

Faculty of technology

Delhi University, Delhi-11042

DELHI COLLEGE OF ENGINEERING

## DELHI- 110042

Website: www.dceonline.net

Fax: (9111) 27871023

Phone: 011-27871018, 27871013

Place: Delhi

Certificate

This is to certify that the major project report entitled “ANALYSIS OF Si-Mo S.G. IRON MANUFACTURING TECHNIQUES & THE EFFECTS OF HEAT TREATMENT ON ITS MICROSTRUCTURE USING  IMAGE ANALYSIS TECHNIQUE” which is being submitted by Mr.Rishi Kant in partial fulfillment of the requirements for the award of the degree of Master of Engineering (Production) of Delhi College of Engineering, Delhi is a record of his own work carried out by him under my supervision and guidance. The matter embodied in this minor project report has not been submitted elsewhere for the award of any degree.

GUIDE

Shri. Vijay Gautam

Senior Lecturer

Department of Mechanical Engineering

Date:                                                                   	                                        Place

Acknowledgements

I would like to express my profound and most sincere appreciation for my guide Prof. Vijay Gautam (Sr. Lecturer) for his careful guidance and continuous encouragement during the entire period of this study. Special thanks go to him for giving me an opportunity to work in the leading area of ductile iron manufacturing.

I would like to express a special thanks to Prof. C.K. Dutta, Department of mechanical&production engineering at Delhi College of engineering, for his valuable suggestions at time to time during whole study.

I extent my special thanks to Mr. Mahesh Kumar(Asst. General Manager)  at Rico Auto Ltd. who took pain in making me familiar about ductile iron casting.

It was my great pleasure to work in well equipped metallurgy and welding labs. I would like to thank of Mr. Pradeep and Vinay staff member of these labs, in Mechanical &production engg. Deptt. of Delhi College of Engg..

I extent my deepest gratitude to my father , sister for their invaluable love, affection, encouragement & all jeevan vidya parivaar at IIT,Kanpur& MS3 ,Kanpur for their moral and encourageous support during my study. I feel extremely privileged that I could receive the guidance of Shri Ganesh Bagariaji (Sir),Archana Didi&Shri Kumar Sambhav without whom I could never achieve my understanding and vision of life.

Rishi Kant

Abstract

In prevailing scenario ductile iron has been proved one of the Ferro-alloy that is known for its versatility and higher performance at lower cost than other members of ferrous casting family which often provides the designer with the best combination of overall properties. This versatility is especially evident in the area of mechanical properties where ductile iron offers the designers the option of choosing high ductility, with grades guaranteeing more than 18% elongation, or high strength, with tensile strength exceeding 825 MPa [2]. The ductile iron family is comprised of Spheroidal graphite nodules embedded in matrices such as ferrite, pearlite, tempered martensite or austenite.

The Si Mo Spheroidal cast iron is new development of ductile iron family on which attention is focused presently.

Here an attempt has been made for sorting out the best manufacturing process for this type of ductile iron among all manufacturing process for its wide application in automotive industry.

The procedure allows further relations with process reliability and product quality. Concerning the matrix, ferrite and pearlite contents were evaluated; concerning graphite, the size, shape and number of the spheroids were determined. Spheroidal cast iron images were obtained by specially developed casting experiments and by analysis of industrial case.

Here the possibility for enhancement in mechanical properties after normalizing of Si Mo Spheroidal cast iron sample is made by correlating the change in phases & grain size distribution. The change in mechanical properties of Si-Mo iron sample after normalizing is being predicted and verified after testing. The analysis is based on image processing technique by using image analysis software named as GAIA BLUE 5.2, GAIA MATERIAL5.3.

Key words: ductile iron, manufacturing process, phases, image analysis, nodularity.

Contents

Certificate                  	ii

Acknowledgements	iii

Abstract	iv-v

Contents	vi

List of Figures	vii-x

Chapter 1 Introduction                                                                       	1-7

1.1 Introduction	1-2

1.2 Background	2-6

1.3 Why Si Mo Spheroidal cast iron	6

1.4 Objective of present work:	6-7

Chapter2 Literature Review	8-28

2.1 Inoculation of Cast Iron	8-11

2.2 Primary carbides in ductile cast iron	11-13

2.3 Effect of silicon	14-15

2.4 Effect of Molybdenum	15-16

2.5 Comparison between ductile iron and carbon steel	16-19

2.6 Influencing Factors Ductile Iron Production	20

2.7 Evaluation of ductile iron	21

2.7.1 Unique properties of magnesium	21

2.7.2 Different treatment process	22

2.7.3 Nodularity and nodule count	23-26

2.8.4 Fading of magnesium and rare earths	26-28

Chapter 3 About digital image and software used	29-44

Chapter 4 Phase analysis of ductile iron	45-80

4.1 An overview of graphite nodularity	30-33

Chapter 5 Conclusion and Scope of Future Work	81-82

5.1.Conclusion	81-82

5.2 Scope of future work	82

Chapter 6 references	83-84

List of figure

Figure1.1: worldwide growth of ductile iron production, 1950-2000

Figure 2.1 poor ductile iron nodularity (100x, unetched)

Figure 2.2 unfavorable graphitic nodules (100x, unetched)

Figure 2.3 Ductile iron microstructure, pearlite (dark constituents) and ferrite (white constituents, white platelets are primary carbide from inadequate inoculation (400x, nital etched).

Figure 2.4 Ductile iron microstructure shows flake surface graphite (400x, nital etched)

Figure 2.5 Ductile iron microstructure illustrates poor graphite nodularity (400x, nital etched)

Figure 2.6 Ductile iron microstructure illustrates Ferritic matrix (400x, nital etched)

Figure 2.7 Ductile iron photomicrographs with a Ferritic matrix showing white angular constituents within ferrite are primary carbides (400x, nital etched).

Figure 2.8 Ductile iron photomicrographs with a Ferritic matrix showing white angular constituents within ferrite are primary carbides (400x, nital etched).

Figure 2.9 Ductile iron photomicrographs illustrating primary carbides in Pearlitic ductile iron (400x, nital etched).

Figure 2.10 Ductile iron photomicrographs illustrating primary carbides in Pearlitic ductile iron (400x, nital etched).

Figure 2.11 photomicrograph of normalized Ferritic ductile iron (200x, nital etched).

Figure 2.12 iron iron-iron carbide-silicon ternary diagram, sectioned at 2% silicon

Source: iron casting hand book, American cast metals association.

Figure 2.13 effect on silicon content on the critical temperature of cast iron

Figure 2.14 influence of molybdenum on the minimum creep rate of Ferritic ductile iron

Figue 2.15 effect of molybdenum on the stress-rupture behavior of Ferritic ductile iron

Figure 2.17 vibration damping characteristics of different material

Figure2.18. Relationship between final sulfur and magnesium affected by other factors

Figure 2.19 Mg and rare earth combination and graphite shapes.

Figure 2.20 Graphite shapes, Mg and rare earth levels

Figure 2.21. Fading of Mg, Ce and La in treated iron reheated in the furnace as well as held in a covered ladle, sampled periodically in a 16 minute total time interval.

Figure 3.1 (from ductile iron data) [1]

Figure3.2 schematic diagram of ductile iron casting production [19]

Figure3.3 showing step by step ductile iron cylinder manufacturing

Figure3.4 sandwich cover ladle

Figure3.5 Tundish cover ladle [6]

Figure3.6 sketch of original tundish cover ladle.

Figure3.6A Fixed tundish cover ladle[6]

Figure3.7: second generation fixed top tundish ladle[6]

Figure 3.8: Tea pot ladles[6]

Figure 3.9 : second type tea pot ladle

Figure 3.10 : double tea pot type tundish ladle[6]

Figure 3.11: Lifting cover design[6]

Figure 3.12: in-mould process[6]

Figure4.1  Phase analysis dialogue box

Figure 4.2  sample 1

Figure 4.3  sample2

Figure 4.4 Wet polishing equipment

Figure4.5 Electric furnace used for heat treatment

Figure 4.6 showing sample at 890±°C during heat treatment

Figure4.9 Grain Nodule at 200x showing Ferritic matrix

Figure-4.10 Grain Nodule at 200x showing Ferritic matrix etched with 2% nital

Figure-4.11 Grain Nodule at 200x showing Ferritic matrix

Figure-4.12.Grain Nodule at 400x-1 etched with 2% nital

Figue.4.13Grain Nodule at 400x-2 etched with 2% natal

Figure4.14 Grain Nodule at 400x-3 etched with 2% natal

Figure4.16 showing nodules at 100x before etching

Figure4.17 showing ASTM grain size

Figure4.18 Graphite analysis of sample microstructure before heat treatment

Figure.4.20 Phase analysis of sample microstructure before heat treatment

Figure.4.21   At 100x showing graphitic nodules before etching At 100x after etched with 2% nital showing grains

Figure 4.22At 200x after etched with 2% nital showing grains At 400x after etching showing grains

Figure4.23 Grain size analusis

Figure 4.25 Graphite analysis of sample microstructure after heat treatment

Figure4.26 Grain size distribution

Figure 4.27 Phase analysis of sample after heat treatment

Figure 4.28 Iteration 2 for % phase count

Chapter 1

Introduction

1.1 Introduction

The material which has low cost, design flexibility, good machinability, high strength-to-weight ratio, good toughness, wear resistance, fatigue strength has been remain the prime requirement of the designer. In this context ductile Iron (Spheroidal cast Iron or nodular Iron) has been proved the best material to fulfill all above requirements from last fifty years.

Alloy ductile irons containing 4-6% silicon and 0.4-2% molybdenum (a special type of S.G.Iron) is used to meet the increasing demands for high strength ductile irons capable of operating at high temperatures in applications such as exhaust manifolds or turbocharger castings. The primary properties required for such applications are oxidation resistance, structural stability, strength and resistance to thermal cycling [1].

These unalloyed grades retain their strength to moderate temperatures; perform well under low to moderate severity thermal cycling and exhibit resistance to growth and oxidation that is superior to that of unalloyed Gray Iron. Alloying with silicon and molybdenum significantly improves the high temperature performance of ferritic Ductile Irons while maintaining many of the production and cost advantages of conventional Ductile Irons[1].

Effect of silicon and molybdenum on the high temperature tensile and creep rupture strengths of ferritic Ductile Iron are shown in the table below

| Material | Tensile Strength MPa | Stress Rupture MPa |
| --- | --- | --- |
|  | 426ºC | 537º C | 650º C | 1000hr@537º C |
| Gray Iron | 370 | 250 | 120 | 590 |
| 60-40-18 D.I. | 400 | 250 | 130 | 830 |
| 4% Si D.I. | 560 | 360 | 130 | 1000 |
| 4% Si - 1% Mo D.I. | 610 | 440 | 190 | 1400 |
| 4% Si - 2% Mo D.I. | 650 | 460 | 200 | 170 |

Source: www.Specialtycastings.com

Table 1.1[25]

1.2 Background

Ductile iron is not a single material, but a family of versatile cast iron exhibiting a wide range of properties which are obtained through micro-structural control. The most important and distinguishing feature of all types of ductile iron is the presence of graphite nodules which act as “crack arresters “and give ductile iron ductility, toughness and strength superior to all other cast iron, and equal to many cast and forged steels. It was first developed at Nickel Company Research Laboratory in 1948 by Keith Dwight Mills [1]. He made addition of copper magnesium alloy in ladle to melted cast iron. Due to this treatment of magnesium alloy –the solidified casting contained not flakes but nearly perfect spheres of graphite then ductile iron was born!

| Characteristic | Ductile iron | Malleable iron | Grey iron | 0.3%C cast steel | White iron |
| --- | --- | --- | --- | --- | --- |
| Castability |  |  |  |  |  |
| Ease at machining |  |  |  |  | NA |
| Vibration damping |  |  |  |  |  |
| Surface hardenability |  |  |  |  | NA |
| Modulus of elasticity |  |  |  |  | NA |
| Impact resistance |  |  |  |  | NA |
| Corrosion resistance |  |  |  |  |  |
| Strength/weight |  |  |  |  | NA |
| Wear resistance |  |  |  |  |  |
| Cost of manuf. |  |  |  |  |  |

Where…………….

| Colour | Property status |
| --- | --- |
|  | Best |
|  | Very good |
|  | Good |
|  | worst |

Table: 1.2[1]

A comparison is made among the various materials’ mechanical properties above in table. During the years of ductile iron history from the early 1950s a range of different treatment processes has been developed. Some were found acceptable while others are rejected a long time ago. Some of the early processes involve lance injection and stirring of the ladle, but most of these are not seen in foundries any more. The most widespread processes

today are the group involving over pouring of an MgFeSi-alloy in some kind of treatment ladle. The growth in ductile iron production world wide is depicted below in figure1.

Figure1.1: worldwide growth of ductile iron production, 1950-2000[1]

Types of ductile iron[1]

- Ferritic ductile iron: Graphite spheroids in a matrix of ferrite provide an iron with good ductility and impact resistance and with a tensile and yield strength equivalent to low carbon steel. Ferritic ductile iron may be produced as cast but may given an annealing heat treatment to assure maximum ductility& low temperature toughness.

- Ferritic-Pearlitic ductile iron: These are most common grade of ductile iron and are normally produced in the as cast condition. The graphite spheroids are in a matrix containing both ferrite and pearlite. Mechanical properties of this type of

ductile iron lie between ferritic and pearlitic ductile iron with good machinability and low production cost.

65-45-12                                     80-55-06                                         100-70-02

(Ferritic ductile iron)           (Ferritic-Pearlitic ductile iron)           Pearlitic ductile iron

Figure 1.2 types of ductile iron[19]

- Pearlitic ductile iron: Graphite spheroids in a matrix of pearlitic result in an iron with high strength, good wear resistance, moderate ductility and impact resistance. Machinability is also superior to steels.

The preceding three type of ductile iron is most common and are usually used in the as cast condition. But ductile iron can also be alloyed or heat treated to provide following grades for wide variety additional applications.

- Martensitic ductile iron: using sufficient alloy to prevent pearlitic formation and a quench and temper heat treatment produces this type of ductile iron. The resultant tempered martensite matrix develops very high strength and wear resistance but with lower level of ductility and toughness.

- Bainitic ductile iron: This grade can be obtained through alloying or heat treatment to produce a hard, wear resistance material.

- Austenitic ductile iron: Alloyed to produce an austenitic matrix, this ductile iron offers good corrosion and oxidation resistance, good magnetic properties and good strength and dimensional stability at elevated temperature.

- Austempered ductile iron (ADI): ADI is the most recent addition to ductile iron family, is a sub-group of ductile iron produced by giving conventional ductile iron a special austempering heat treatment. Nearly twice as strong as pearlitic ductile iron.ADI still retains high elongation and toughness. This combination provides a material with superior wear resistance and fatigue strength.

1.3 Why Si Mo Spheroidal cast iron

The mechanical properties of Si Mo Spheroidal cast iron has been found nearly to steel (>0.35% C) i.e. medium carbon steel due to its Ferritic matrix. This material provides properties like oxidation resistance, structural stability& resistance to thermal cycling at lower cost with more design flexibility than steel. Steel grades having less than 0.35% carbon are usually carburized before they can be heat-treated. A fully pearlitic matrix or even a highly pearlitic one offers suitable wear resistance in the as cast state and can sometimes replace carburized and heat-treated steel, depending on the application[].

That is why in present scenario S.G. Iron is replacing the place of steel from the material world, for further enhancement in its mechanical properties it has created a lot of interest for research.

1.4 Objective of present work:

Mechanical properties of Spheroidal cast iron are influenced by a great number of a variables as a result of the melting process; in general, they depend on the chemical composition of the melt, the physical state of the liquid iron as well as on the cooling rate of the casting [17]. Among the available tests for evaluating the properties of nodular cast iron products, the micrographic analysis is still of primary importance, due to the basic and irreplaceable information it provides about the shape and the distribution of both nodules and matrix. It is a qualitative inspection by size, degree of roundness and distribution of nodules [16].

This thesis reports about best manufacturing techniques for production of Si Mo Spheroidal cast iron & shows the changes occurred through measuring phases, nodules, grain size etc. in mechanical properties of Si Mo Spheroidal cast iron’s sample after normalizing.

The sole aim of this thesis is to correlate the % of phases (ferrite, pearlite etc.), grain size to mechanical properties of the sample after heat treatment.

chapter 2

literature review

2.1 Ductile iron

Ductile iron, also known as spheroidal graphite (S.G.) iron or nodular iron is made by treating liquid iron of suitable composition with magnesium before casting. This promotes the precipitation of graphite in the form of discrete nodules instead of interconnected flakes. The nodular iron so formed has high ductility, allowing castings to be used in critical applications such as: Crankshafts, steering knuckles, differential carriers, brake calipers, hubs, brackets, valves, water pipes, pipe fittings and many others. Ductile iron production now accounts for about 40% of all iron castings and is still growing [1,2].

Having high carbon equivalent value (CEV) and very low sulphur, sufficient magnesium is added to the liquid iron to give a residual magnesium content of about 0.04%, the iron is inoculated and cast. The graphite then precipitates in the form of spheroids. It is not easy to add magnesium to liquid iron. Magnesium boils at a low temperature (1090°C), so there is a violent reaction due to the high vapor pressure of Mg at the treatment temperature causing violent agitation of the liquid iron and considerable loss of Mg in vapor form[3]. This gives rise to the familiar brilliant ‘magnesium flare’ during treatment accompanied by clouds of white magnesium oxide fume. During Mg treatment, oxides and sulphides are formed in the iron, resulting in dross formation on the metal surface; this dross must be removed as completely as possible before casting. The residual magnesium in the liquid iron after treatment oxidizes continuously at the metal surface, causing loss of magnesium which may affect the structure of the graphite spheroids; moreover the dross formed may result in harmful inclusions in the castings.

The first step introduces a nodulizing agent, such as magnesium, which creates the condition for the graphite to precipitate and grow in a nodular shape. If insufficient Mg is added, or if the molten metal is held for an extended period after the Mg has been added, the graphite will not precipitate in a round shape. Figures1and2 show unacceptable graphite nodularity that was identified in the cover plate for a floor-level utility box in a major convention center. The designated material for this cover was ASTM A536-80, Grade 65-45-12 ductile cast iron [3]. The second critical processing step is to add an inoculant. The inoculant is usually a ferrosilicon that contains small amounts of calcium and/or aluminum and other special-purpose elements.

The principal purpose of the inoculant is to prevent chill.

Figure 2.1 poor ductile iron nodularity                                    figure 2.2 unfavorable graphitic nodule (100x,unetched)

More using the covers from the floor-level utility boxes as examples, Figs. 3, 4 and 5 illustrate the presence of primary carbides in a Ferritic structure and in structures that contain both ferrite and pearlite. These utility box covers failed immediately after installation, due to the movement of heavy equipment across them. The ductile iron covers that met the A536-80 requirements for 65-45-12 ductile iron grade performed acceptably without failure [3]. The presence of the degenerate graphite illustrated in Figs. 2.1 and 2.2 impairs mechanical properties. The presence of primary carbides in the structure can also reduce mechanical properties. In both instances, the ductility, as measured by the percent elongation, is most dramatically reduced. The observed structures can be the consequence of fade. Fade occurs when the effects of Mg treatment and inoculation decrease with time. If the molten metal is held for an extended period after Mg treatment and inoculation, both degenerate graphite and primary carbides can occur in the structure. Another possibility for the observed structures could be high sulfur-base iron contaminated with deleterious trace elements [3].

figure 2.3                                                                   figure 2.4

figure 2.5                                                                            figure 2.6

2.2 Primary carbides in ductile cast iron

Ductile cast iron is particularly prone to the formation of primary carbides during solidification. A primary reason for this susceptibility is that the graphite forms into a spherical shape, which is the lowest surface area-to-volume ratio for the graphite. The limited surface area available for graphite precipitation, during solidification, increases the carbide-forming tendency. In addition, the principle element added for the nodulizing treatment is Mg, a known carbide stabilizer. Another factor is that the S content in ductile iron is purposely lowered to less than 0.02%, to facilitate the formation of spherical graphite nodules[10]. Therefore, inoculation is crucial to successfully cast ductile iron without carbides. Even after effective inoculation, fade can occur and result in the formation of primary carbides. Figures 2.6, 2.7 and 2.8 are three different examples of primary carbides in a ferritic ductile iron. These carbides have several names, including ledeburite, chill, primary carbide, Fe3C, iron carbide cementite, white iron and hard iron. The principle step in controlling the occurrence of primary carbides in ductile iron calls for close attention to detail concerning inoculation and fade time. The effects of inoculation fade with time and, therefore, processing time within the foundry should be closely controlled. In many instances, modern-day foundries have utilized late-stream inoculation or mold inoculation to counteract effects of fade.

figure 2.7                                                                               figure 2.8

figure 2.9                                                                 figure 2.10

By heat treating ductile iron Pearlitic content increases the microstructure normalized ductile is shown below in figure 2.11.

Figure 2.11

2.3 Effect of silicon

Silicon enhances the performance of ductile iron at elevated temperatures by stabilizing the Ferritic matrix and forming a silicon rich surface which inhibits oxidation. Stabilization of the ferrite phase reduces high temperature growth in tow ways .firstly, silicon raises the critical temperature at which ferrite transforms to austenite which have been shown below in figure. The critical temperature is considered to be the upper limit of useful temperature range for Ferritic docile iros.seondly silicon has strongly fertilizing tendency which stabilizes matrix against the formation of carbides.[1]

Figure 2.12 iron iron-iron carbide-silicon ternary diagram, sectioned at 2% silicon

Source: iron casting hand book, American cast metals association[1]

Effect of Sion  critical temperature in cast iron

Figure 2.13 effect on silicon content on the critical temperature of cast iron[1]

Source: ductile iron data by www.ductile.org

2.4Effect of Molybdenum

Molybdenum restricts the creep and stress rupture propogation.the addition of 0.5% molybdenum to Ferritic ductile iron produces significant increases in creep and stress rupture strengths. The different effects of molybdenum as shown below in figure.

Figure 2.14 influence of molybdenum on the minimum creep rate of Ferritic ductile iron[1]

Figue 2.15 effect of molybdenum on the stress-rupture behavior of Ferritic ductile iron[1].

2.5Comparison between ductile iron and carbon steel

Cast irons can be produced to a fully pearlitic matrix, which is an advantage over carbon steel. Approximately 1% carbon is required to produce an essentially pearlitic matrix. Most carbon steels commercially produced have between 0.10% to 0.80% so there is a limit to the amount of pearlite that can be obtained in the matrix. In order to achieve maximum wear resistance steel has to be heat-treated. Carbon steel grades having less than 0.35% carbon are usually carburized before they can be heat-treated. A fully pearlitic matrix or even a highly pearlitic one offers suitable wear resistance in the as cast state and can sometimes replace carburized and heat-treated steel, depending on the application.

65-45-12                               80-55-06                           100-70-02

Figure 2.16

The property requirements for an application are very important in selecting the best grade of ductile iron for an application. Carbon steels are designated by chemical composition. Ductile iron is designated by the minimum tensile strength, yield strength and elongation. Besides tension properties, torsion strength, shear strength, modulus of elasticity, impact properties and heat treat response are just a few material characteristics that may also need to be considered.

The chemical composition of carbon steel affects mechanical properties. High carbon steels will have higher tensile strengths, lower elongation, decreased machinability and better response to heat-treat than low carbon steels. Additions of sulfur, manganese, phosphorus and lead are commonly used to improve machinability, usually at the expense, to some degree, of strength.    The amount of carbon dissolved in iron determines the amount of pearlite in the matrix which influences most of the mechanical properties, heat-treat response and machinability. Elements such as sulfur and phosphorus form sulfides and phosphides that do not dissolve in iron and make carbon steel "free machining".

Ductile iron has carbon levels that exceed the solubility limit in iron. At 2800F, approximately 6% carbon is soluble in iron. At the eutectic point, only 2% can remain in solution and the excess carbon is precipitated into a graphite nodule. The precipitated graphite is a solid phase, which promotes the same benefits as the inclusions deliberately put in carbon steels. Ductile iron bars are free machining and drilled holes require less deburing.

Ductile irons with relatively low levels of combined carbon will have a matrix consisting primarily of ferrite. They have the lowest tensile strength and wear resistance, highest elongation and usually will be the easiest to machine. The level of combined carbon can be increased to produce a matrix that is fully pearlitic which results in higher tensile strengths and wear resistance, lowest elongation and will be more difficult to machine. The ratio of pearlite to ferrite in the matrix will produce ductile iron grades that have properties somewhere between those with a fully pearlitic or fully ferritic matrix.

Figure 2.17 vibration damping characteristics of different material[20]

Vibration damping is important in gears and in applications where harmonic vibrations cause failure. In an automotive balance shaft, gear noise reduction resulted directly from the conversion of 1144 steel to 80-55-06 ductile iron without any change in how the part was being manufactured. The 4140 pistons in an impact hammer were cracking prematurely because of harmonic vibrations. The failures stopped when the part was converted to austempered ductile iron(heat treated at 870ºC followed by quenching and again heat treated at 300ºC). Although the ductile iron had lower tensile strengths, the vibration damping characteristics reduced harmonic vibrations and the conversion was a success.

The best way to select ductile iron in comparison to steel is to match the matrix structure as close as possible. Usually a ferritic ductile will be the best candidate to replace carbon steels having up to .35% carbon. Partially pearlitic ductile irons such as an 80-55-06 are the best candidates for the medium carbon steels. Fully pearlitic ductile irons are best for replacing carbon steels that require heat treat to improve wear resistance. The machinability of a fully pearlitic ductile may be less than the carbon steel but the savings from eliminating all the steps associated with heat treat can offset the additional cost of machining[20].

2.6 Influencing Factors Ductile Iron Production

The experiments done by ductile iron society reveals the factor effecting the ductile iron microstructure by different element which are given below in table.

| Element | Segregation Factor (FS) | Pearlite Promoting Effectiveness (FP) | Intercellular Graphite Promotion | Chunky Graphite Promotion | Carbides Promotion |
| --- | --- | --- | --- | --- | --- |
| C |  |  |  |  |  |
| Si | 0.7 |  |  | X |  |
| Mn | 1.7-3.5 | 0.44 |  |  | X |
| P | 2.0 | 5.60 |  |  |  |
| S |  |  | X |  |  |
| Ni | 0.3 | 0.37 |  | X |  |
| Cu | 0.1 | 4.90 | X |  |  |
| Ti | 25.0 | 4.40 | X |  | X |
| V | 13.2 | X |  |  | X |
| Cr | 11.6 | 0.37 |  |  | X |
| Co | 0.4 |  |  |  |  |
| Sn |  | 39.0 | X |  |  |
| Mo | 25.3 | 7.90 |  |  | X |
| Bi |  |  | X |  |  |
| Pb |  |  | X |  |  |
| Sb |  | X | X |  |  |
| As |  | X | X |  |  |
| Cd |  |  | X |  |  |
| Al |  |  | X |  |  |
| Mg |  |  |  |  | X |
| Ce |  |  |  | X | X |
| Ca |  |  |  | X |  |
| Zn |  |  | X |  |  |
| Zr |  |  | X |  |  |
| N |  | X |  |  |  |
| B |  |  |  |  | X |
| H |  |  |  |  | X |
| Se |  |  |  |  | X |
| Te |  |  |  |  | X |

Table 2.1 The Specific Group of Elements in Ductile Iron[20]

2.7 Evaluation of ductile iron

The result of ductile iron conversion from steel scrap followed by inoculation is measured or evaluated by the following factors:

- Nodularity - maximize

- Nodule count - maximize

- Chill carbides - minimize

- Inverse chill - minimize

- Shrinkage porosity- minimize

- Inclusions - minimize

2.7.1 Unique properties of magnesium

Magnesium has a low boiling point, high reactivity with oxygen and low solubility in iron making reliable additions to iron difficult. To minimize Mg reactivity calcium is added to the master alloy. Magnesium content of the alloy is also restricted to lower the reactivity. To increase solubility silicon is raised in the vicinity of the alloy by using ferrosilicon as cover material. To satisfy different needs many alloys were developed with combinations of Mg and rare earths.

2.7.2 Different treatment process
Many different treatment processes have evolved over the years to achieve better quality ductile iron at the lowest cost. Many variables affected the selection of a particular treatment process. Some of the factors are:

- Base melt quality including sulfur content

- Temperature of treatment, holding and pouring

- Delays in metal handling

- Casting section modulus

- Ease of late inoculation

These factors affect the treatment technique due to the unique properties of magnesium and resulted in the following processes, which are still used in commercial production:

- Open ladle

- Tundish

- Flow thru processes

- Pure magnesium processes-Converters, plunging, pressure vessels

- Wire feeders

- In-mold process

2.7.3 Nodularity and nodule count

It has been shown by many that the nodule shape is best when the magnesium residual is just enough as too much will deteriorate the nodule shape from fully spheroidal. Nodule count can be maximized by sound base iron melting practice and good inoculation practice. Cooling rate affects both the nodule count and the nodule shape. Fast solidifying iron results in better nodule shape than slowly cooled iron for the same magnesium residuals. Larger sections require increased magnesium residual and late inoculation reduces the magnesium requirement. When rare earths are added to the iron the amount of magnesium required is also reduced. As some of the magnesium measured is in the form of magnesium sulfide, final iron sulfur level affects the magnesium needed to result in nodular graphite[21]. All of these effects are shown in the figure 1.

Figure2.18. Relationship between final sulfur and magnesium affected by other factors [21]

Combination of rare earths and magnesium Over the years it was noticed that some tramp elements affected the graphite shape. Increasing magnesium was not able to counteract the effect of tramp elements like Pb, Ti, Bi etc. Rare earths were found to neutralize these elements and restore the graphite shape to nodular form. Hence rare earths were added either with or incorporated in master alloys. For irons treated with pure magnesium Rare Earths could be added as mish metal or rare earth containing inoculants. Rare earths, like magnesium, will combine with sulfur and oxygen. They are also additive to magnesium in nodularizing effect. Because of this, one has to look at magnesium and rare earths content in total and not separately in determining amounts needed for best properties. As the rare earths are heavier than magnesium it takes 5.8 times more rare earths than magnesium, by weight, to combine with sulfur and oxygen.

The Atomic weights of rare earths are about 140, and that of magnesium is 24. Combination of magnesium and rare earths resulting in various shapes of graphite is shown in figure 2.19 When rare earths are added with magnesium alloy the analyzed rare earths include that portion combined with oxygen and sulfur, similar to magnesium analysis[21].

Figure 2.19 Mg and rare earth combination and graphite shapes[21].

Types and amount of rare earths in the magnesium alloy varied over the years depending on the economics. As rare earths are more expensive than magnesium alloy and it takes quite bit more to combine with oxygen and sulfur it is necessary to examine the relationship of rare earths in ductile iron manufacturing. There is much anecdotal information regarding the use of rare earths and its effect on the graphite shape. A minimum amount is necessary to neutralize any residual tramp elements that may be present in the iron. It has been shown that proper addition of rare earths increase nodule count. When cerium in the magnesium alloy is used in excess resulting in a residual of over 0.01%, pro-eutectoid graphite particles tend to be larger and may result in graphite floatation and exploded graphite, especially when the sulfur is low and the CE is on the high side. When rare earths are added after the magnesium treatment along with the stream inoculant then the level of cerium that causes graphite nodule enlargement and floatation is much lower than the 0.01%. It is closer to 0.004%. The difference may be due to the fact that the rare earths in the first case are combined with sulfur and oxygen and most of the rare earths are uncombined in solution in the second case. This will lead one to envision the magnesium and rare earth relationship differently if the rare earths are added after the magnesium treatment where most of the oxygen and sulfur are tied up with magnesium. This may be represented in the revised areas for various shapes of graphite in figure 2.20. Obviously the levels of Mg and rare earths do not stay the same throughout the pour in a batch system due to fading of active elements with time. From figure 3 there is no vermicular graphite shown when there is no rare earths in the iron. Ductile iron with only magnesium will revert to grey iron without going through a vermicular graphite form[21].

Figure 2.20 Graphite shapes, Mg and rare earth levels

2.7.4 Fading of magnesium and rare earths

Fading of the elements Mg and rare earths (mainly Ce, La and Pr) is due to several factors. Magnesium can evaporate due to high vapor pressure at the melt temperatures. Both Mg and rare earths will react with combined oxygen present in the iron as oxides of Si, Mn and Fe. Sulfides of these elements breakdown to form oxides and the freed sulfur will react with free Mg and rare earths. All of these mechanisms are active in any treated ductile iron melt[21].

The rate of fading will increase if the iron bath contains high amounts of slag, if the temperature of the melt is high and the if the melt is exposed to turbulence either in the furnace, or in the ladle when it is tilted back and forth. Protective atmospheres and clean full ladles held without disturbances minimize fading as shown in figure 4. Due to this fading event, treated iron needs to be poured before the levels of Mg and rare earths fall below that necessary for the castings being poured.

If the iron is held in a pressure pour furnace under nitrogen or inert atmosphere, the iron will have a longer life. In pressure pour furnaces sulfur tends to be lower due to the time factor hence magnesium level could be lower and still produce good ductile iron. Of course the late inoculation in the form of stream inoculation helps to improve nodularity, which helps in reducing the level of magnesium.

One of the problems seen in the industry is if pouring ladles are not emptied at the end of pouring, the remaining iron cools down and solidifies as grey iron. This may cause problems for the next time as this iron will fade faster than normal[21].

Inoculant fading is different from magnesium fading. Inoculant fading results in lower nodule count, chilled edges (carbides) and inverse chill. It can also result in lower nodularity even when there is adequate Mg and rare earths for the section thickness and sulfur levels.

Each foundry should establish the maximum time the iron can be poured for their circumstances.

Figure 2.21. Fading of Mg, Ce and La in treated iron reheated in the furnace as well as held in a covered ladle, sampled periodically in a 16 minute total time interval[21].

Chapter 3

Analysis of manufacturing techniques

3.1 Silicon molybdenum ductile iron

Alloy ductile irons containing 46% silicon and 0.4-2% molybdenum is used to meet the increasing demands for high strength ductile irons capable of operating at high temperatures in applications such as exhaust manifolds or turbocharger castings. The primary properties required for such applications are oxidation resistance, structural stability, strength and resistance to thermal cycling[1].

These unalloyed grades retain their strength to moderate temperature fig 3.1 perform well under low to moderate severity thermal cycling, ferritic ductile irons exhibit less growth at high temperatures due to the stability of the microstructure alloying with silicon molybdenum significantly improves the high temperature performance of Ferritic ductile iron while maintaining many of the production and cost advantages of conventional ductile irons.

Figure 3.1 (from ductile iron data) [1]

3.2common Manufacturing process of ductile iron:

Figure3.2 schematic diagram of ductile iron casting production [19]

Figure(a) Figure(b) Figure(c) Figure(d) Figure(e) Figure(f) Figure(g) Figure(h) Figure(i) Figure1.3 showing step by step ductile iron cylinder manufacturing

3.2 MAGNESIUM TREATMENT PROCESSES

Different manufacturing processes are given below:

- Over pour or sandwich

- Tundish cover

- In the mould

- Flow through

- Cored wire

Magnesium recovery: since magnesium reacts with all of sulphur present in the base metal by considering this effect, magnesium recovery is calculated as (theoretically):

% of magnesium recovery=

Where = (initial sulphur content-final sulphur content)[1]

3.2.1 THE SANDWICH COVER PROCESS

The term sandwich is derived from the fact that a covering material or sandwich layer is added on top of the spheroidizing alloy prior to the addition of molten iron to retard the start of alloy reaction [6]. A 1% to 2% addition of steel punching is most widely used as cover material although other material as ferrosilicon is also used. In addition to the delaying action, the cover material cools the metal in the immediate vicinity of the magnesium reaction.

Figure3.4 sandwich cover ladle

This cooling effect takes advantage of the fact that magnesium recovery increases as the metal temperature decreases. Recovery of magnesium is normally fairly good with the sandwich treatment and may range up to 50-60 per cent. Advantages are short treatment times, simplicity, flexibility, and the improved recovery with less slag and fumes. The disadvantages are slightly greater temperature loss due to the additional heat required to melt the 1% to 2% cover materials.

3.2.2 THE TUNDISH COVER PROCESS

Magnesium losses to MgO are greatly reduced because no new oxygen can enter the ladle once the filling orifice of the tundish is covered with metal. Magnesium recoveries can be as high as 70-75%, a considerable improvement over the plain sandwich method.

In the early development stages of the tundish ladle, production foundries were encouraged by the improved magnesium efficiency but discouraged by the need to continually replace the cover with each treatment. This drawback was overcome by incorporating a semi-permanent, bolted-on cover or a separate lifting lug system that did not have to be removed after each treatment. Figure 3.5 shows an example of a simple tundish cover ladle design. Preferentially, the height: width ratio of the ladle should be at least 2:1, with larger ratios improving the process even more. The optimum treatment vessel for a tundish cover process will be like a long tube divided vertically for lining maintenance. The tundish cover process is suitable for all treatment sizes ranging from 100 kgs to 10 tonnes[6].

Figure3.5 Tundish cover ladle [6]

The tundish cover lid may be designed to suit a range of different foundry conditions. Examples are fixed lid, automatic lift or manual removable lid. The metal outlet from the lid should be sized to suit the amount of iron being treated. When a divider wall or alloy chamber is applied, the metal stream must fall into the part of the bottom not containing the alloy. By such a process, very high recoveries and good process consistency can easily be obtained provided the right alloy is applied. Consequently, low levels of fume and smoke will escape from the vessel, giving a good foundry environment.

An advantage for this process concept is the design of two symmetric alloy chambers at the bottom of the ladle. By such dual alloy chambers, the ladle can be more or less self cleaning with respect to slag built-up. The self cleaning is done by shifting between alloy charging and pouring in both chambers. As the alloy chamber is growing with slag, the lid is shifted 180° and the clean pouring chamber is then applied for the alloy. The slag contaminated alloy chamber will then be cleaned out again by the hot and turbulent metal stream when located directly under the tundish hole[6].

For all kinds of sandwich and tundish processes it is an advantage to apply a charging tube equipped with a funnel when placing the alloy into the ladle. By lowering the tube into the alloy pocket and fill the alloy through it, spilling into the other chamber is avoided. Also, the sandwich cover material will be better positioned over the alloy when charged through such a tube.

(a)Tundish Ladle Design - Fixed Top

Figure 3 shows some alternative ways of designing tundish cover ladles with fixed lid.

Side view                                                 Top view

Figure3.6 sketch of original tundish cover ladle.

A fixed lid requires an alloy charging port for introduction of MgFeSi-alloy. Also, it is recommended to put the alloy in a pocket at the opposite side of the ladle bottom to where the metal stream hits during filling.

Figure3.6 Fixed tundish cover ladle[6]

Ladles with fixed lid can generally not be deslagged, and therefore slag accumulation may be a problem during time. Hence, low slag forming alloys (low Ca, Al and RE) is recommended for such ladles to minimize slag formation inside the ladle.

Figure3.7: second generation fixed top tundish ladle[6]

(b)Tundish Ladle Design - Tea Pot Ladles

The tea pot ladles offers an advantage in that liquid iron can be filled through the tea pot spout. This means that the tundish cover basin is eliminated.

Figure 3.8: Tea pot ladles[6]

Both fixed and removable lids can be applied for tea pot ladles. For ladles operating with a single spout, there is a possible risk that the last iron will not pick up magnesium.

Figure 3.9 : second type tea pot ladle

This iron will stay in the spout until teeming, and if used directly into a mould it may be undertreated or even grey iron. To avoid such problems a double teapot with a separate filling and pouring spout can be designed.

Figure 3.10 : double tea pot type tundish ladle[6]

Tea pot ladles will generally supply cleaner metal into pouring ladles and auto pours due to the slag skimming effect of the spout. Figure 4 shows examples of tea pot ladles.

(c)Tundish Ladle Design - Lifting Cover

The lifting or removable Tundish cover design is probably the most flexible and easiest to maintain. Lifting covers can be either integrated to the ladle with a separate lifting lug or constructed as a fully removable lid by using for instance a fork lift truck. The lid can also be mounted onto the furnace spout. The major advantages with removable lids are easy deslagging and cleaning of the ladles and also that the same lid can be used for several ladles. Charging of MgFeSi-alloy is also easier when the lid is removed from the ladle top. As shown in Figure 3.11, there exist a range of alternative ways to design a tundish cover ladle, but common for all is that most foundries can make the lid in their own foundry workshop at low costs.

Figure 3.11: Lifting cover design[6]

Each foundry has to decide from their own possibilities and limitations which type of lid is the most suitable. There will always be room for own creativity in designing and modifying the suggested alternatives. The main importance is to include some kind of cover to the treatment ladle thereby improving process economics and metal cleanliness, and significantly reducing smoke and fume emission.

3.2.3 THE IN-MOULD PROCESS

In the mould is a process for spheroidizing the molten iron within the mould itself. A special reaction chamber is incorporated within the runner and gating system of the mould, as shown in Figure3.12. Spheroidizing alloys are placed in the chamber, and the reaction occurs during the pouring process. As expected, the process requires precise control to produce optimum spheroidization and good castings. A controlled reaction between the metal and the alloy depends on a number of conditions including metal temperature, stream velocity, alloy shape, and casting size and geometry.

Figure 3.12: in-mould process[6]

Magnesium recoveries of 70-80% are typical. It is absolutely essential that the sulphur is kept at 0.01% or below before treatment to minimize the chance of inclusion defects. Pouring times must be carefully controlled to ensure that there is alloy being dissolved throughout the entire filling sequence.

The disadvantage of a lower casting yield is apparent because the reaction chamber is a part of each runner system. The increased possibility of slag and other reaction products to enter the casting is also a disadvantage. There probably is a greater need for testing nodularity of every casting produced due to the fact that each mould is a separate treatment. An advantage is elimination of the need for subsequent inoculation addition since the process itself gives a very good nucleation effect.

3.2.4 THE FLOW THROUGH PROCESS

The flow through process or external stream treatment process is a patented spin-off from the mould treatment method and also is external to the mould and ladle. Alloy is placed in a reaction chamber over which the molten iron passes and reacts with the alloy. The dimensions of the chamber are critical to achieve successful treatment. Because the reaction chamber is of predetermined dimensions, wide variations in sulphur levels cannot be tolerated. Magnesium recoveries of 30-50% are reported. The need for a lower magnesium containing alloy with somewhat restrictive sizing may negatively impact the overall economics.

3.2.5 THE CORED WIRE PROCESS

Over the last few years, cored wire has increased its popularity for nodularization of ductile iron. Normally, the hollow wire tube is filled with either magnesium metal or a high magnesium containing alloy. This wire is then injected into the liquid iron by a feeding machine. Advantages are reported to be predictable Mg recovery, availability to desulphurize and magnesium treat in one ladle, tailor made wire chemistry to fit individual applications, greater silicon level flexibility in base iron. Normal magnesium recoveries are found to be between 30-50%. Disadvantages are large amounts of slag and fume associated with a very violent reaction. Also, the inoculation effect may be largely reduced by the violent reaction since many of the nuclei are separated[6].

Chapter 4

EXPERIMENTATION

4.1 About digital image and software used

Digital image: Digital image may be defined as “it is a function of two real variables I=f(x, y)” .we can take an example the intensity of brightness (I) in (x,y) co-ordinate system. at different position image will have different intensity of brightness.

GAIA Blue is a representative Image Analysis Tool, can be used for capturing image, and image adjustment also be done like brightness, contrast etc.

After refining an image the phase and graphite analysis can be done through GAIA MATERIAL, which is inbuilt software in GAIA BLUE. Some control functions are given bellow:

Some control functions of GAIA MATERIAL is given below:

Figure4.1  Phase analysis dialogue box

4.2 Grain Size Plainimetric Method for grain size analysis

International Standard For measuring grain size is ASTM E 112.

Number of Grain per sqr mm : NA = the number of grains which exist in 1 squre

millimeter area.

ASTM grain size number(G) : Average grain size based on ASTM E112. The equation is followed

Average of Inner Grain Size: Average of inner grain size based on real area in second column of grain table.

Average of Border Grain Size: Average of outer grain size based on real area in second column of grain table.

Average of Grain Size: Average of total grain size based on real area in second column of grain table.

4.3 EXPERIMENTAL SET UP & PROCEDURE

Some samples of different components in as cast condition were obtained from industry to perform experiments. The possibility for further enhancement in these sample’s mechanical properties by heat treatment has been studied here.

The samples were prepared by dry polishing the surface of specimens with various grades of polish papers of silicon carbide (water-proof), starting with 220, 320, 400 and 600. After this the specimens were polished on rotating disc with paste of alumina (Al2O3) abrasive powder (fine size of 6µm), water were used as coolants. Finally the specimens were etched by 2% nital (Containing 98 mm3 ethanol and 2 mm3 nitric acid) and then washed off with water. Then the specimens were dried by means of blower and the microstructure of specimen was recorded by means of metallurgical microscope attached with CCD camera.

Sample1 chemical composition

| C | Si | Mn | Mg | Cu | Mo | Hardness |
| --- | --- | --- | --- | --- | --- | --- |
| 3.3 | 3.82 | 0.305 | 0.054 | 0.09 | 0.905 | 205 |

Sample 2 chemical composition

| C | Si | Mn | Mg | Cu | Mo | Hardness |
| --- | --- | --- | --- | --- | --- | --- |
| 3.1 | 4.05 | 0.223 | 0.045 | 0.062 | 0.57 | 216 |

Dry Polished samples

Figure 4.2                              		                               Figure 4.3

Experimentation: Machines used in Metallurgical and welding Laboratory, Delhi College of Engineering, Delhi-42.

Figure 4.4 Wet polishing equipment                                 figure4.5    Electric furnace used for heat treatment

Wet polishing Equipment:

Manufacturer: Metatech Industries limited, Delhi.

R.P.M of polishing wheel: 2800

Heat treatment furnace:

Furnace Type: Electric arc furnace

Manufacturer:  Metatech Industries limited, Delhi

Max. Temperature of furnace: 1350ºC.

Figure 4.6 showing sample at 890±°C during heat treatment

4.4 Heat Treatment Cycle for sample

Figure 4.8

The average of heating rate is found 5.933ºC by this furnace and average cooling rate is found to 22.25ºC.

The holding time has been maintained for 90 minutes in the austenitic range.

4.5Image processing set up

Image display device       Inverted metallurgical

Microscope

Figure.4.8.A.Manufacturer Onix Vision Technologies private limited

285, Sector 21-A, Faridabnad-121001

Haryana (India)

4.6 Microstructures before performing heat treatment on sample

Figure4.9 Grain Nodule at 200x showing Ferritic matrix                Figure-4.10 Grain Nodule at 200x showing Ferritic matrix etched with 2% nital

Figure-4.11 Grain Nodule at 200x showing Ferritic matrix   Figure-4.12.Grain Nodule at 400x-1 etched with 2% nital

Figue.4.13Grain Nodule at 400x-2 etched with 2% nital        Figure4.14  Grain Nodule at 400x-3 etched with 2% nital

Figure4.16 showing nodules at 100x before etching

4.7 Grain analysis before heat treatment

The grain analysis of sample microstructure has been done with help of image analysis software the typical window has been shown below in figure during working

Figure4.17 showing ASTM grain size

| No. | Area | Length | ASTM G |  | No. | Area | Length | ASTM G |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 314.09 | 84.079 | 8.687 |  | 45 | 734.51 | 114.767 | 7.461 |
| 1 | 90.16 | 38.359 | 10.487 |  | 46 | 55.86 | 31.819 | 11.178 |
| 2 | 70.56 | 55.159 | 10.841 |  | 47 | 367.01 | 88.068 | 8.462 |
| 3 | 271.95 | 81.548 | 8.894 |  | 48 | 165.62 | 55.839 | 9.61 |
| 4 | 167.09 | 50.139 | 9.597 |  | 49 | 686.49 | 115.757 | 7.558 |
| 5 | 808.5 | 133.518 | 7.322 |  | 50 | 332.71 | 86.838 | 8.603 |
| 6 | 481.67 | 87.248 | 8.07 |  | 51 | 287.63 | 74.788 | 8.813 |
| 7 | 12.25 | 14.87 | 13.367 |  | 52 | 138.67 | 42.489 | 9.866 |
| 8 | 193.06 | 72.129 | 9.389 |  | 53 | 128.38 | 40.749 | 9.977 |
| 9 | 17.15 | 17.67 | 12.881 |  | 54 | 393.47 | 93.357 | 8.361 |
| 10 | 9.8 | 25.9 | 13.689 |  | 55 | 392 | 95.408 | 8.367 |
| 11 | 792.82 | 131.687 | 7.351 |  | 56 | 93.1 | 40.919 | 10.441 |
| 12 | 10.78 | 25.08 | 13.551 |  | 57 | 586.53 | 104.027 | 7.786 |
| 13 | 8.33 | 21.7 | 13.923 |  | 58 | 337.12 | 71.848 | 8.584 |
| 14 | 5.88 | 14.7 | 14.426 |  | 59 | 128.87 | 43.719 | 9.972 |
| 15 | 105.35 | 39.83 | 10.263 |  | 60 | 123.97 | 45.359 | 10.028 |
| 16 | 240.1 | 67.999 | 9.074 |  | 61 | 468.44 | 96.808 | 8.11 |
| 17 | 5.39 | 13.3 | 14.551 |  | 62 | 81.83 | 38.359 | 10.627 |
| 18 | 153.37 | 51.639 | 9.721 |  | 63 | 228.34 | 62.188 | 9.147 |
| 19 | 314.09 | 89.778 | 8.687 |  | 64 | 30.87 | 19.289 | 12.033 |
| 20 | 101.92 | 39.859 | 10.31 |  | 65 | 103.88 | 40.269 | 10.283 |
| 21 | 172.48 | 51.059 | 9.551 |  | 66 | 23.03 | 16.44 | 12.456 |
| 22 | 23.03 | 16.03 | 12.456 |  | 67 | 279.3 | 71.988 | 8.856 |
| 23 | 34.3 | 20.399 | 11.881 |  | 68 | 65.66 | 31.239 | 10.945 |
| 24 | 140.14 | 48.909 | 9.851 |  | 69 | 852.11 | 122.517 | 7.247 |
| 25 | 195.02 | 65.059 | 9.374 |  | 70 | 177.38 | 51.978 | 9.511 |
| 26 | 387.1 | 80.289 | 8.385 |  | 71 | 2.94 | 3.79 | 15.426 |
| 27 | 307.72 | 70.348 | 8.716 |  | 72 | 824.18 | 133.017 | 7.295 |
| 28 | 7.35 | 8.45 | 14.104 |  | 73 | 190.61 | 56.108 | 9.407 |
| 29 | 520.38 | 131.186 | 7.958 |  | 74 | 69.58 | 32.759 | 10.861 |
| 30 | 68.11 | 37.369 | 10.892 |  | 75 | 270.97 | 74.718 | 8.9 |
| 31 | 12.74 | 20.689 | 13.31 |  | 76 | 413.07 | 96.518 | 8.291 |
| 32 | 86.73 | 33.869 | 10.543 |  | 77 | 346.92 | 87.248 | 8.543 |
| 33 | 171.01 | 49.079 | 9.564 |  | 78 | 121.03 | 44.278 | 10.062 |
| 34 | 83.3 | 33.679 | 10.601 |  | 79 | 133.77 | 53.329 | 9.918 |
| 35 | 97.51 | 41.089 | 10.374 |  | 80 | 52.92 | 29.719 | 11.256 |
| 36 | 12.74 | 14.17 | 13.31 |  | 81 | 16.66 | 15.04 | 12.923 |
| 37 | 182.28 | 55.959 | 9.472 |  | 82 | 122.01 | 43.769 | 10.051 |
| 38 | 542.43 | 98.858 | 7.898 |  | 83 | 53.41 | 28.319 | 11.243 |
| 39 | 187.18 | 62.358 | 9.433 |  | 84 | 206.29 | 60.159 | 9.293 |
| 40 | 216.58 | 55.619 | 9.223 |  | 85 | 17.64 | 14.75 | 12.841 |
| 41 | 147.49 | 45.459 | 9.777 |  | 86 | 188.65 | 58.809 | 9.422 |
| 42 | 580.16 | 116.097 | 7.801 |  | 87 | 168.07 | 55.499 | 9.589 |
| 43 | 122.01 | 51.519 | 10.051 |  | 88 | 57.82 | 27.859 | 11.128 |
| No. | Area | Length | ASTM G |  | No. | Area | Length | ASTM G |
| 89 | 85.75 | 58.639 | 10.56 |  | 133 | 52.92 | 26.749 | 11.256 |
| 90 | 708.54 | 112.377 | 7.513 |  | 134 | 98.49 | 40.439 | 10.36 |
| 91 | 32.83 | 21.099 | 11.945 |  | 135 | 44.59 | 25.179 | 11.503 |
| 92 | 57.33 | 30.539 | 11.14 |  | 136 | 196 | 60.859 | 9.367 |
| 93 | 32.83 | 20.64 | 11.945 |  | 137 | 541.94 | 93.428 | 7.9 |
| 94 | 85.26 | 36.889 | 10.568 |  | 138 | 531.65 | 101.368 | 7.927 |
| 95 | 361.62 | 75.468 | 8.483 |  | 139 | 158.27 | 55.888 | 9.675 |
| 96 | 205.31 | 55.329 | 9.3 |  | 140 | 1077.02 | 155.496 | 6.909 |
| 97 | 99.96 | 40.099 | 10.338 |  | 141 | 87.71 | 36.309 | 10.527 |
| 98 | 447.37 | 88.238 | 8.176 |  | 142 | 18.62 | 17.599 | 12.763 |
| 99 | 343.49 | 81.138 | 8.557 |  | 143 | 19.11 | 17.31 | 12.725 |
| 100 | 234.71 | 63.319 | 9.107 |  | 144 | 13.72 | 12.65 | 13.203 |
| 101 | 227.36 | 62.839 | 9.153 |  | 145 | 82.32 | 40.149 | 10.618 |
| 102 | 63.21 | 42.149 | 10.999 |  | 146 | 10.78 | 11.66 | 13.551 |
| 103 | 379.26 | 82.778 | 8.415 |  | 147 | 25.48 | 19.289 | 12.31 |
| 104 | 514.01 | 97.218 | 7.976 |  | 148 | 10.29 | 10.26 | 13.618 |
| 105 | 36.75 | 31.889 | 11.782 |  | 149 | 272.44 | 61.998 | 8.892 |
| 106 | 97.51 | 39.449 | 10.374 |  | 150 | 98 | 42.319 | 10.367 |
| 107 | 295.96 | 66.558 | 8.772 |  | 151 | 130.34 | 52.459 | 9.955 |
| 108 | 33.81 | 22.379 | 11.902 |  | 152 | 58.8 | 28.799 | 11.104 |
| 109 | 75.95 | 35.149 | 10.735 |  | 153 | 72.03 | 29.959 | 10.811 |
| 110 | 164.15 | 51.978 | 9.623 |  | 154 | 64.68 | 32.859 | 10.966 |
| 111 | 286.65 | 70.348 | 8.818 |  | 155 | 304.29 | 71.508 | 8.732 |
| 112 | 142.1 | 44.469 | 9.831 |  | 156 | 31.85 | 22.259 | 11.988 |
| 113 | 426.79 | 85.028 | 8.244 |  | 157 | 19.11 | 15.57 | 12.725 |
| 114 | 337.61 | 71.438 | 8.582 |  | 158 | 69.58 | 31.869 | 10.861 |
| 115 | 32.83 | 19.24 | 11.945 |  | 159 | 173.46 | 52.289 | 9.543 |
| 116 | 92.61 | 38.769 | 10.448 |  | 160 | 168.07 | 53.258 | 9.589 |
| 117 | 63.21 | 30.61 | 10.999 |  | 161 | 167.09 | 58.229 | 9.597 |
| 118 | 48.51 | 27.979 | 11.381 |  | 162 | 182.77 | 55.259 | 9.468 |
| 119 | 102.9 | 48.259 | 10.296 |  | 163 | 122.01 | 49.829 | 10.051 |
| 120 | 70.07 | 37.519 | 10.851 |  | 164 | 92.12 | 39.109 | 10.456 |
| 121 | 300.86 | 78.048 | 8.749 |  | 165 | 25.48 | 23.27 | 12.31 |
| 122 | 15.19 | 13.81 | 13.057 |  | 166 | 62.72 | 30.61 | 11.011 |
| 123 | 33.32 | 22.789 | 11.923 |  | 167 | 69.09 | 38.119 | 10.871 |
| 124 | 721.28 | 112.407 | 7.487 |  | 168 | 318.01 | 81.958 | 8.669 |
| 125 | 34.79 | 21.22 | 11.861 |  | 169 | 641.41 | 112.477 | 7.656 |
| 126 | 73.5 | 36.309 | 10.782 |  | 170 | 99.47 | 38.119 | 10.345 |
| 127 | 791.84 | 143.327 | 7.353 |  | 171 | 91.63 | 47.509 | 10.464 |
| 128 | 1021.65 | 163.507 | 6.985 |  | 133 | 52.92 | 26.749 | 11.256 |
| 129 | 5.88 | 6.76 | 14.426 |  | 134 | 98.49 | 40.439 | 10.36 |
| 130 | 232.75 | 75.418 | 9.119 |  | 135 | 44.59 | 25.179 | 11.503 |
| 131 | 324.87 | 72.978 | 8.638 |  | 136 | 196 | 60.859 | 9.367 |
| 132 | 18.62 | 16.199 | 12.763 |  | 137 | 541.94 | 93.428 | 7.9 |

Final analyzed table

| Contents | Value |
| --- | --- |
| Field Area | 49674.24 per sqr mm |
| Total Number | 223 |
| Number of Inner | 166 |
| Number of Border | 57 |
| Real Number | 194.5 |
| Number of Grain per sqr mm | 3915.51 |
| ASTM grain size number(G) | 8.985 |
| Average of Inner Grain Size | 204.153 |
| Average of Border Grain Size | 182.142 |
| Average of Grain Size | 198.527 |

4.8 Measurement of Nodularity in ductile cast iron [7]

Spheroidal (nodular or ductile) graphite iron  SGI, has an as-cast structure containing graphite particles in the form of small rounded, “Spheroidal”, “globular” or “nodular” particles in a ductile metallic matrix. It has been established that all of the mechanical and

physical properties characteristic of SGI are a result of the graphite being substantially or

wholly in the spheroidal/nodular shape such that its bulk physico-mechanical properties are determined primarily by the steel-like matrix. Any departure from this shape or a proportion of the graphite will cause a drastic deviation from these properties. Occasionally, a consistent Spheroidal type of graphite is not obtained in regular production of ductile iron. This may result from insufficient or excessive nodulariser, or non-uniform treatment or the presence of inhibiting elements. Also, the problem may be the choice of nodulariser, mode of addition, and environmental and/or human considerations. However, unlike other renowned engineered materials, requirements concerning graphite “spheroidicity” in SGI seldom appear in users’ specifications. In essence, commercial SGI castings are designed on the basis of their properties and rarely on the basis of their graphite morphology, shape or structure. Graphite nodularity, usually evaluated by visual assessment, might be utilized as a simple form of selection for castings to determine which should and should not be accepted[7] . The adoption of a uniform and universally acceptable structure-property specification for SGI by international standard organizations and societies is still a long way in the future. For now, the techniques used in assessing the graphite nodularity or spheroidicity in commercial SGIs have included visual assessment of structure and recently, the use of special image analyzing microscopes and software.

4.9 AN OVERVIEW OF GRAPHITE NODULARITY

It is a common practice in the field of shape analysis to specify at least two different shape parameters, the first one being a global measure of the particle and the second, concentrating on its morphological details. For graphite particles in the hue of compacted/vermicular, near-nodule and spheroids in cast iron, several parameters have been defined, each serving different purposes in relation to particular properties or features.

Nodularity is defined as [7]:

A particle is considered to be nodular if its aspect ratio is greater than 0.5.

.

Flake graphite is one of seven types (shapes or forms) of graphite established in ASTM A 247. Flake graphite is subdivided into five types (patterns), which are designated by the letters A through E. Graphite size is established by comparison with an ASTM size chart, which shows the typical appearances of flakes of eight different sizes at 100x magnification.

Type A or 0 flake graphite (random orientation) is preferred for most applications. In the intermediate flake sizes, type A flake graphite is superior to other types in certain wear applications such as the cylinders of internal combustion engines.

Type B or 1 flake graphite (rosette pattern) is typical of fairly rapid cooling, such as is common with moderately thin sections (about 10 mm) and along the surfaces of thicker sections, and sometimes results from poor inoculation.

The large flakes of type C or 2 flake graphite are typical of kish graphite that is formed in hypereutectic irons. These large flakes enhance resistance to thermal shock by increasing thermal conductivity and decreasing elastic modulus. On the other hand, large flakes are not conducive to good surface finishes on machined parts or to high strength or good impact resistance.

The small, randomly oriented interdendritic flakes in type D or 3 flake graphite promote a fine machined finish by minimizing surface pitting, but it is difficult to obtain a Pearlitic matrix with this type of graphite. Type D or 3 flake graphite may be formed near rapidly cooled surfaces or in thin sections. Frequently, such graphite is surrounded by a ferrite matrix, resulting in soft spots in the casting.

Type E or 4 flake graphite is an interdendritic form, which has a preferred rather than a random orientation. Unlike type D or 3  graphite, type 6 graphite can be associated with a pearlitic matrix and thus can produce a casting whose wear properties are as good as those of a casting containing only type A or 0 graphite in a pearlite matrix[20].

4.10Graphite analysis of sample microstructure before heat treatment

Figure4.18 Graphite analysis of sample microstructure before heat treatment

| No. | Area | Class | Circularity |
| --- | --- | --- | --- |
| 1 | 1389 | 0 | 0.01 |
| 2 | 47 | 2 | 0.77 |
| 3 | 125 | 1 | 0.71 |
| 4 | 75 | 1 | 0.77 |
| 5 | 31 | 3 | 0.32 |
| 6 | 13 | 4 | 0.62 |
| 7 | 29 | 3 | 0.78 |
| 8 | 124 | 1 | 0.7 |
| 9 | 11 | 4 | 0.52 |
| 10 | 48 | 2 | 0.79 |
| 11 | 144 | 0 | 0.65 |
| 12 | 121 | 1 | 0.68 |
| 13 | 476 | 0 | 0.64 |
| 14 | 55 | 2 | 0.57 |
| 15 | 76 | 1 | 0.59 |
| 16 | 136 | 0 | 0.39 |
| 17 | 19 | 3 | 0.2 |
| 18 | 48 | 2 | 0.49 |
| 19 | 12 | 4 | 0.57 |
| 20 | 58 | 2 | 0.6 |
| 21 | 50 | 2 | 0.82 |
| 22 | 76 | 1 | 0.78 |
| 23 | 170 | 0 | 0.77 |
| 24 | 21 | 3 | 0.57 |

| No. | Area | Class | Circularity |
| --- | --- | --- | --- |
| 25 | 27 | 3 | 0.73 |
| 26 | 37 | 2 | 0.61 |
| 27 | 92 | 1 | 0.71 |
| 28 | 251 | 0 | 0.61 |
| 29 | 106 | 1 | 0.82 |
| 30 | 72 | 1 | 0.74 |
| 31 | 71 | 1 | 0.73 |
| 32 | 85 | 1 | 0.66 |
| 33 | 109 | 1 | 0.84 |
| 34 | 149 | 0 | 0.84 |
| 35 | 38 | 2 | 0.62 |
| 36 | 130 | 0 | 0.73 |
| 37 | 10 | 4 | 0.27 |
| 38 | 25 | 3 | 0.68 |
| 39 | 36 | 2 | 0.16 |
| 40 | 44 | 2 | 0.72 |
| 41 | 171 | 0 | 0.41 |
| 42 | 11 | 4 | 0.52 |
| 43 | 489 | 0 | 0.86 |
| 44 | 333 | 0 | 0.39 |
| 45 | 11 | 4 | 0.52 |
| 46 | 11 | 4 | 0.18 |
| 47 | 99 | 1 | 0.56 |
| 48 | 134 | 0 | 0.61 |
| 49 | 309 | 0 | 0.37 |
| 50 | 177 | 0 | 0.64 |
| 51 | 121 | 1 | 0.55 |
| 52 | 29 | 3 | 0.78 |
| 53 | 180 | 0 | 0.65 |
| 54 | 55 | 2 | 0.57 |
| 55 | 21 | 3 | 0.57 |
| 56 | 147 | 0 | 0.83 |
| 57 | 76 | 1 | 0.59 |
| 58 | 14 | 4 | 0.67 |
| 59 | 406 | 0 | 0.38 |
| 60 | 11 | 4 | 0.52 |
| 61 | 42 | 2 | 0.69 |
| 62 | 56 | 2 | 0.92 |
| 63 | 24 | 3 | 0.65 |
| 64 | 137 | 0 | 0.77 |
| 65 | 183 | 0 | 0.66 |
| 66 | 50 | 2 | 0.52 |
| 67 | 32 | 3 | 0.52 |
| 68 | 95 | 1 | 0.74 |

| No. | Area | Class | Circularity |
| --- | --- | --- | --- |
| 69 | 83 | 1 | 0.47 |
| 70 | 56 | 2 | 0.92 |
| 71 | 240 | 0 | 0.69 |
| 72 | 99 | 1 | 0.28 |
| 73 | 165 | 0 | 0.75 |
| 74 | 199 | 0 | 0.35 |
| 75 | 167 | 0 | 0.76 |
| 76 | 32 | 3 | 0.52 |
| 77 | 44 | 2 | 0.72 |
| 78 | 117 | 1 | 0.91 |
| 79 | 61 | 2 | 1 |
| 80 | 26 | 3 | 0.7 |
| 81 | 54 | 2 | 0.89 |
| 82 | 118 | 1 | 0.67 |
| 83 | 77 | 1 | 0.79 |
| 84 | 11 | 4 | 0.18 |
| 85 | 168 | 0 | 0.76 |
| 86 | 30 | 3 | 0.17 |
| 87 | 13 | 4 | 0.62 |
| 88 | 86 | 1 | 0.49 |
| 89 | 29 | 3 | 0.78 |
| 90 | 138 | 0 | 0.78 |
| 91 | 93 | 1 | 0.96 |
| 92 | 80 | 1 | 0.82 |
| 93 | 28 | 3 | 0.76 |
| 94 | 10 | 4 | 0.48 |
| 95 | 44 | 2 | 0.45 |
| 96 | 33 | 2 | 0.89 |
| 97 | 24 | 3 | 0.39 |
| 98 | 49 | 2 | 0.8 |
| 99 | 17 | 3 | 0.46 |
| 100 | 14 | 4 | 0.67 |
| 101 | 42 | 2 | 0.24 |
| 102 | 72 | 1 | 0.41 |
| 103 | 112 | 1 | 0.87 |
| 104 | 11 | 4 | 0.52 |
| 105 | 288 | 0 | 0.83 |
| 106 | 36 | 2 | 0.59 |
| 107 | 32 | 3 | 0.52 |
| 108 | 131 | 0 | 0.74 |
| 109 | 79 | 1 | 0.61 |
| 110 | 41 | 2 | 0.42 |
| 111 | 39 | 2 | 0.22 |
| 112 | 902 | 0 | 0.63 |

| No. | Area | Class | Circularity |
| --- | --- | --- | --- |
| 113 | 51 | 2 | 0.84 |
| 114 | 211 | 0 | 0.51 |
| 115 | 44 | 2 | 0.45 |
| 116 | 664 | 0 | 0.79 |
| 117 | 31 | 3 | 0.84 |
| 118 | 32 | 3 | 0.52 |
| 119 | 290 | 0 | 0.7 |
| 120 | 98 | 1 | 0.76 |
| 121 | 207 | 0 | 0.59 |
| 122 | 11 | 4 | 0.52 |
| 123 | 108 | 1 | 0.84 |
| 124 | 173 | 0 | 0.78 |
| 125 | 44 | 2 | 0.25 |
| 126 | 77 | 1 | 0.22 |
| 127 | 24 | 3 | 0.65 |
| 128 | 279 | 0 | 0.8 |
| 129 | 157 | 0 | 0.71 |
| 130 | 23 | 3 | 0.62 |
| 131 | 116 | 1 | 0.66 |
| 132 | 136 | 0 | 0.49 |
| 133 | 102 | 1 | 0.29 |
| 134 | 59 | 2 | 0.17 |
| 135 | 141 | 0 | 0.8 |
| 136 | 280 | 0 | 0.43 |
| 137 | 39 | 2 | 0.64 |
| 138 | 137 | 0 | 0.62 |
| 139 | 189 | 0 | 0.46 |
| 140 | 97 | 1 | 0.55 |
| 141 | 13 | 4 | 0.35 |
| 142 | 16 | 4 | 0.26 |
| 113 | 51 | 2 | 0.84 |
| 114 | 211 | 0 | 0.51 |
| 115 | 44 | 2 | 0.45 |
| 116 | 664 | 0 | 0.79 |
| 117 | 31 | 3 | 0.84 |
| 118 | 32 | 3 | 0.52 |
| 119 | 290 | 0 | 0.7 |
| 120 | 98 | 1 | 0.76 |
| 121 | 207 | 0 | 0.59 |
| 122 | 11 | 4 | 0.52 |
| 123 | 108 | 1 | 0.84 |
| 124 | 173 | 0 | 0.78 |
| 125 | 44 | 2 | 0.25 |
| 126 | 77 | 1 | 0.22 |

| No. | Area | Class | Circularity |
| --- | --- | --- | --- |
| 127 | 24 | 3 | 0.65 |
| 128 | 279 | 0 | 0.8 |
| 129 | 157 | 0 | 0.71 |
| 130 | 23 | 3 | 0.62 |
| 131 | 116 | 1 | 0.66 |
| 132 | 136 | 0 | 0.49 |
| 133 | 102 | 1 | 0.29 |
| 134 | 59 | 2 | 0.17 |
| 135 | 141 | 0 | 0.8 |
| 136 | 280 | 0 | 0.43 |
| 137 | 39 | 2 | 0.64 |
| 138 | 137 | 0 | 0.62 |
| 139 | 189 | 0 | 0.46 |
| 140 | 97 | 1 | 0.55 |
| 141 | 13 | 4 | 0.35 |
| 142 | 16 | 4 | 0.26 |
| 127 | 24 | 3 | 0.65 |
| 128 | 279 | 0 | 0.8 |
| 129 | 157 | 0 | 0.71 |
| 130 | 23 | 3 | 0.62 |
| 131 | 116 | 1 | 0.66 |
| 132 | 136 | 0 | 0.49 |
| 133 | 102 | 1 | 0.29 |
| 134 | 59 | 2 | 0.17 |
| 135 | 141 | 0 | 0.8 |
| 136 | 280 | 0 | 0.43 |
| 137 | 39 | 2 | 0.64 |
| 138 | 137 | 0 | 0.62 |
| 139 | 189 | 0 | 0.46 |
| 140 | 97 | 1 | 0.55 |
| 141 | 13 | 4 | 0.35 |
| 142 | 16 | 4 | 0.26 |
| 127 | 24 | 3 | 0.65 |
| 128 | 279 | 0 | 0.8 |
| 129 | 157 | 0 | 0.71 |
| 130 | 23 | 3 | 0.62 |
| 131 | 116 | 1 | 0.66 |
| 132 | 136 | 0 | 0.49 |
| 133 | 102 | 1 | 0.29 |
| 134 | 59 | 2 | 0.17 |
| 135 | 141 | 0 | 0.8 |
| 136 | 280 | 0 | 0.43 |
| 137 | 39 | 2 | 0.64 |
| 138 | 137 | 0 | 0.62 |

Statistics for nodularity

| No | Content | Data |
| --- | --- | --- |
| 1 | Field Area | 101376 sqr um |
| 2 | Nodules per sqr mm | 1302.083 |
| 3 | Nodularity-Count | 92.96% |
| 4 | Nodularity-Area | 84.72% |

4.11Phase analysis of sample microstructure before heat treatment

Figure.4.20 Phase analysis of sample microstructure before heat treatment

Phase data:

| Type of Phase | Analyzed Surface (%) |
| --- | --- |
| Graphite | 14.23 |
| Pearlite | 10.22 |
| Ferrite | 40.45 |
| Carbide | 34.81 |
| Other | 0.29 |

4.12Microstructures after performing heat treatment on sample

Figure.4.21   At 100x showing graphitic nodules before etching                    At 100x after etched with 2% nital showing grains

Fugure 4.22At 200x after etched with 2% nital showing grains                 At 400x after etching showing grains

4.13 Grain analysis after heat treatment

At 200x                                                            Analyzed picture

Figure4.23 Grain size analusis

| No. | Area | Length | ASTM G |  | No. | Area | Length | ASTM G |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 550 | 106.698 | 7.878 |  | 50 | 1131 | 140.953 | 6.838 |
| 1 | 944 | 130.255 | 7.099 |  | 51 | 83 | 34.213 | 10.607 |
| 2 | 127 | 41.142 | 9.993 |  | 52 | 492 | 95.012 | 8.039 |
| 3 | 915 | 124.74 | 7.144 |  | 53 | 1066 | 145.853 | 6.924 |
| 4 | 746 | 125.225 | 7.439 |  | 54 | 1766 | 182.154 | 6.195 |
| 5 | 80 | 32.899 | 10.66 |  | 55 | 59 | 29.385 | 11.099 |
| 6 | 511 | 95.77 | 7.984 |  | 56 | 923 | 128.74 | 7.131 |
| 7 | 372 | 79.083 | 8.442 |  | 57 | 253 | 59.527 | 8.999 |
| 8 | 12 | 16.414 | 13.397 |  | 58 | 197 | 57.77 | 9.36 |
| 9 | 16 | 12.071 | 12.982 |  | 59 | 117 | 39.042 | 10.111 |
| 10 | 138 | 43.284 | 9.873 |  | 60 | 233 | 66.213 | 9.117 |
| 11 | 6 | 7.828 | 14.397 |  | 61 | 98 | 39.728 | 10.367 |
| 12 | 114 | 44.314 | 10.149 |  | 62 | 493 | 95.468 | 8.036 |
| 13 | 424 | 89.184 | 8.254 |  | 63 | 845 | 125.497 | 7.259 |
| 14 | 56 | 31.485 | 11.174 |  | 64 | 1420 | 160.397 | 6.51 |
| 15 | 510 | 101.77 | 7.987 |  | 65 | 250 | 73.669 | 9.016 |
| 16 | 1604 | 178.397 | 6.334 |  | 66 | 679 | 99.083 | 7.574 |
| 17 | 230 | 59.728 | 9.136 |  | 67 | 94 | 32.556 | 10.427 |
| 18 | 537 | 100.355 | 7.913 |  | 68 | 2820 | 206.137 | 5.52 |
| 19 | 260 | 68.355 | 8.959 |  | 69 | 647 | 94.912 | 7.644 |
| 20 | 50 | 26.899 | 11.338 |  | 70 | 1248 | 156.882 | 6.696 |
| 21 | 535 | 100.255 | 7.918 |  | 71 | 290 | 66.113 | 8.802 |
| 22 | 418 | 99.326 | 8.274 |  | 72 | 1025 | 122.255 | 6.98 |
| 23 | 513 | 86.698 | 7.979 |  | 73 | 77 | 31.042 | 10.715 |
| 24 | 213 | 64.456 | 9.247 |  | 74 | 73 | 33.385 | 10.792 |
| 25 | 119 | 56.314 | 10.087 |  | 75 | 815 | 121.669 | 7.311 |
| 26 | 289 | 69.527 | 8.807 |  | 76 | 460 | 81.284 | 8.136 |
| 27 | 401 | 91.527 | 8.334 |  | 77 | 612 | 105.083 | 7.724 |
| 28 | 72 | 34.899 | 10.812 |  | 78 | 155 | 44.556 | 9.705 |
| 29 | 818 | 120.497 | 7.306 |  | 79 | 65 | 27.314 | 10.959 |
| 30 | 864 | 116.983 | 7.227 |  | 80 | 138 | 42.456 | 9.873 |
| 31 | 102 | 38.971 | 10.309 |  | 81 | 311 | 73.012 | 8.701 |
| 32 | 248 | 63.426 | 9.027 |  | 82 | 113 | 39.87 | 10.161 |
| 33 | 216 | 55.042 | 9.227 |  | 83 | 365 | 83.426 | 8.47 |
| 34 | 13 | 11.071 | 13.281 |  | 84 | 878 | 118.983 | 7.203 |
| 35 | 22 | 13.485 | 12.522 |  | 85 | 489 | 90.113 | 8.048 |
| 36 | 45 | 26.556 | 11.49 |  | 86 | 60 | 26.314 | 11.075 |
| 37 | 43 | 23.314 | 11.555 |  | 87 | 747 | 116.497 | 7.437 |
| 38 | 268 | 76.497 | 8.915 |  | 88 | 8 | 7.414 | 13.982 |
| 39 | 148 | 48.556 | 9.772 |  | 89 | 250 | 59.184 | 9.016 |
| 40 | 582 | 95.225 | 7.797 |  | 90 | 1626 | 192.439 | 6.314 |
| 41 | 925 | 122.497 | 7.128 |  | 91 | 48 | 24.314 | 11.397 |
| 42 | 119 | 43.799 | 10.087 |  | 92 | 90 | 35.627 | 10.49 |
| 43 | 393 | 80.012 | 8.363 |  | 93 | 188 | 59.284 | 9.427 |
| 44 | 224 | 68.527 | 9.174 |  | 94 | 259 | 61.042 | 8.965 |
| 45 | 17 | 11.657 | 12.894 |  | 95 | 318 | 66.426 | 8.669 |
| 46 | 332 | 77.527 | 8.607 |  | 96 | 261 | 68.941 | 8.954 |
| 47 | 246 | 61.87 | 9.039 |  | 97 | 829 | 129.468 | 7.286 |
| 48 | 727 | 109.426 | 7.476 |  | 98 | 168 | 51.556 | 9.589 |

| No. | Area | Length | ASTM G |  | No. | Area | Length | ASTM G |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 99 | 188 | 56.213 | 9.427 |  | 197 | 630 | 94.598 | 7.682 |
| 100 | 829 | 134.497 | 7.286 |  | 198 | 28 | 17.314 | 12.174 |
| 101 | 600 | 104.497 | 7.753 |  | 199 | 787 | 132.782 | 7.361 |
| 102 | 243 | 60.456 | 9.057 |  | 200 | 140 | 48.971 | 9.852 |
| 103 | 421 | 83.426 | 8.264 |  | 201 | 118 | 40.213 | 10.099 |
| 104 | 313 | 73.426 | 8.692 |  | 202 | 2711 | 207.368 | 5.577 |
| 105 | 41 | 30.657 | 11.624 |  | 203 | 841 | 142.296 | 7.266 |
| 106 | 481 | 91.042 | 8.072 |  | 204 | 296 | 90.154 | 8.772 |
| 107 | 456 | 97.598 | 8.149 |  | 205 | 1205 | 138.882 | 6.747 |
| 108 | 497 | 91.426 | 8.024 |  | 206 | 872 | 132.539 | 7.213 |
| 109 | 358 | 94.113 | 8.498 |  | 207 | 268 | 69.77 | 8.915 |
| 110 | 460 | 85.912 | 8.136 |  | 208 | 156 | 57.799 | 9.696 |
| 111 | 74 | 31.385 | 10.772 |  | 209 | 415 | 84.012 | 8.285 |
| 112 | 55 | 26.314 | 11.2 |  | 210 | 1348 | 158.782 | 6.585 |
| 113 | 47 | 24.899 | 11.427 |  | 211 | 92 | 35.042 | 10.458 |
| 114 | 114 | 50.456 | 10.149 |  | 212 | 260 | 68.184 | 8.959 |
| 115 | 100 | 34.314 | 10.338 |  | 213 | 1495 | 155.61 | 6.436 |
| 116 | 602 | 115.468 | 7.748 |  | 214 | 219 | 62.527 | 9.207 |
| 117 | 93 | 35.385 | 10.442 |  | 215 | 837 | 125.196 | 7.272 |
| 118 | 62 | 28.314 | 11.027 |  | 216 | 262 | 60.698 | 8.948 |
| 119 | 509 | 97.184 | 7.99 |  | 217 | 482 | 114.711 | 8.069 |
| 120 | 333 | 73.527 | 8.602 |  | 218 | 27 | 15.485 | 12.227 |
| 121 | 186 | 54.941 | 9.442 |  | 219 | 88 | 37.971 | 10.522 |
| 122 | 694 | 117.669 | 7.543 |  | 220 | 508 | 94.426 | 7.993 |
| 123 | 24 | 14.899 | 12.397 |  | 221 | 584 | 91.669 | 7.792 |
| 124 | 628 | 103.711 | 7.687 |  | 222 | 110 | 46.799 | 10.2 |
| 125 | 639 | 107.083 | 7.662 |  | 223 | 78 | 34.899 | 10.696 |
| 126 | 196 | 56.456 | 9.367 |  | 224 | 617 | 105.326 | 7.712 |
| 127 | 178 | 54.698 | 9.506 |  | 225 | 634 | 102.569 | 7.673 |
| 128 | 990 | 145.539 | 7.03 |  | 226 | 304 | 72.284 | 8.734 |
| 129 | 779 | 124.054 | 7.376 |  | 227 | 693 | 109.811 | 7.545 |
| 130 | 901 | 127.426 | 7.166 |  | 228 | 1162 | 138.811 | 6.799 |
| 131 | 29 | 17.071 | 12.124 |  | 229 | 548 | 94.255 | 7.884 |
| 132 | 122 | 39.385 | 10.051 |  | 230 | 382 | 72.598 | 8.404 |
| 133 | 139 | 47.042 | 9.863 |  | 231 | 131 | 55.698 | 9.948 |
| 134 | 1528 | 163.811 | 6.404 |  | 232 | 335 | 81.083 | 8.594 |
| 135 | 332 | 78.598 | 8.607 |  | 233 | 832 | 114.74 | 7.281 |
| 136 | 367 | 76.355 | 8.462 |  | 234 | 348 | 99.912 | 8.539 |
| 137 | 476 | 99.77 | 8.087 |  | 235 | 197 | 54.213 | 9.36 |
| 138 | 1590 | 224.208 | 6.347 |  | 236 | 779 | 127.296 | 7.376 |
| 139 | 1619 | 176.439 | 6.321 |  | 237 | 68 | 32.314 | 10.894 |
| 140 | 759 | 120.539 | 7.414 |  | 238 | 139 | 43.042 | 9.863 |
| 141 | 53 | 29.385 | 11.254 |  | 239 | 14 | 12.828 | 13.174 |
| 142 | 1410 | 156.711 | 6.52 |  | 240 | 780 | 126.539 | 7.374 |
| 143 | 362 | 78.113 | 8.482 |  | 241 | 738 | 118.397 | 7.454 |
| 144 | 211 | 58.799 | 9.26 |  | 242 | 188 | 57.042 | 9.427 |
| 145 | 1889 | 188.924 | 6.098 |  | 243 | 251 | 65.012 | 9.01 |
| 146 | 664 | 115.184 | 7.607 |  | 244 | 24 | 15.657 | 12.397 |
| 147 | 49 | 26.243 | 11.367 |  | 245 | 45 | 24.899 | 11.49 |

| No. | Area | Length | ASTM G |  | No. | Area | Length | ASTM G |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 246 | 316 | 72.698 | 8.678 |  | 295 | 24 | 15.142 | 12.397 |
| 247 | 158 | 45.042 | 9.678 |  | 296 | 967 | 149.095 | 7.064 |
| 248 | 585 | 107.225 | 7.789 |  | 297 | 1081 | 153.125 | 6.903 |
| 249 | 225 | 62.698 | 9.168 |  | 298 | 314 | 69.284 | 8.687 |
| 250 | 53 | 28.556 | 11.254 |  | 299 | 586 | 88.841 | 7.787 |
| 251 | 265 | 60.941 | 8.932 |  | 300 | 255 | 64.527 | 8.987 |
| 252 | 249 | 74.941 | 9.022 |  | 301 | 376 | 73.284 | 8.427 |
| 253 | 225 | 60.284 | 9.168 |  | 302 | 300 | 61.87 | 8.753 |
| 254 | 804 | 133.326 | 7.331 |  | 303 | 559 | 103.983 | 7.855 |
| 255 | 165 | 60.77 | 9.615 |  | 304 | 1073 | 164.024 | 6.914 |
| 256 | 216 | 61.77 | 9.227 |  | 305 | 326 | 68.941 | 8.633 |
| 257 | 238 | 64.456 | 9.087 |  | 306 | 2139 | 211.066 | 5.919 |
| 258 | 782 | 113.326 | 7.371 |  | 307 | 247 | 61.284 | 9.033 |
| 259 | 574 | 95.083 | 7.817 |  | 308 | 304 | 76.255 | 8.734 |
| 260 | 11 | 9.243 | 13.522 |  | 309 | 270 | 67.184 | 8.905 |
| 261 | 554 | 98.941 | 7.868 |  | 310 | 123 | 44.456 | 10.039 |
| 262 | 510 | 84.841 | 7.987 |  | 311 | 697 | 100.255 | 7.537 |
| 263 | 238 | 66.598 | 9.087 |  | 312 | 46 | 23.728 | 11.458 |
| 264 | 719 | 108.941 | 7.492 |  | 313 | 585 | 107.083 | 7.789 |
| 265 | 501 | 85.184 | 8.013 |  | 314 | 470 | 92.255 | 8.105 |
| 266 | 979 | 137.083 | 7.046 |  | 315 | 501 | 91.012 | 8.013 |
| 267 | 345 | 80.355 | 8.551 |  | 316 | 15 | 12.071 | 13.075 |
| 268 | 203 | 61.728 | 9.316 |  | 317 | 552 | 94.284 | 7.873 |
| 269 | 1153 | 168.61 | 6.81 |  | 318 | 127 | 44.456 | 9.993 |
| 270 | 1053 | 158.296 | 6.941 |  | 319 | 333 | 75.598 | 8.602 |
| 271 | 176 | 52.87 | 9.522 |  | 320 | 78 | 35.385 | 10.696 |
| 272 | 62 | 30.071 | 11.027 |  | 321 | 151 | 51.042 | 9.743 |
| 273 | 208 | 54.941 | 9.281 |  | 322 | 1375 | 164.539 | 6.556 |
| 274 | 25 | 15.485 | 12.338 |  | 323 | 315 | 72.012 | 8.682 |
| 275 | 172 | 62.284 | 9.555 |  | 324 | 830 | 114.74 | 7.285 |
| 276 | 822 | 115.983 | 7.299 |  | 325 | 159 | 50.284 | 9.669 |
| 277 | 610 | 102.154 | 7.729 |  | 326 | 472 | 90.598 | 8.099 |
| 278 | 894 | 124.196 | 7.177 |  | 327 | 701 | 108.598 | 7.528 |
| 279 | 2168 | 179.154 | 5.899 |  | 328 | 400 | 77.527 | 8.338 |
| 280 | 423 | 87.426 | 8.257 |  | 329 | 242 | 61.284 | 9.063 |
| 281 | 376 | 75.841 | 8.427 |  | 330 | 845 | 142.196 | 7.259 |
| 282 | 1620 | 170.539 | 6.32 |  | 331 | 706 | 114.054 | 7.518 |
| 283 | 138 | 42.799 | 9.873 |  | 332 | 1049 | 144.196 | 6.947 |
| 284 | 82 | 32.314 | 10.624 |  | 333 | 838 | 122.154 | 7.271 |
| 285 | 836 | 124.497 | 7.274 |  | 334 | 46 | 24.899 | 11.458 |
| 286 | 465 | 83.184 | 8.12 |  | 335 | 634 | 90.497 | 7.673 |
| 287 | 1459 | 173.267 | 6.471 |  | 336 | 1632 | 186.196 | 6.309 |
| 288 | 348 | 88.527 | 8.539 |  | 337 | 1037 | 141.326 | 6.963 |
| 289 | 1103 | 143.326 | 6.874 |  | 338 | 257 | 68.355 | 8.976 |
| 290 | 304 | 72.941 | 8.734 |  | 339 | 267 | 65.527 | 8.921 |
| 291 | 272 | 62.355 | 8.894 |  | 340 | 376 | 81.698 | 8.427 |
| 292 | 1277 | 146.267 | 6.663 |  | 341 | 227 | 60.113 | 9.155 |
| 293 | 300 | 63.385 | 8.753 |  | 342 | 14 | 13.485 | 13.174 |
| 294 | 638 | 101.083 | 7.664 |  | 343 | 194 | 63.627 | 9.382 |

| No. | Area | Length | ASTM G |  | No. | Area | Length | ASTM G |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 344 | 120 | 39.627 | 10.075 |  | 393 | 478 | 89.083 | 8.081 |
| 345 | 412 | 83.627 | 8.295 |  | 394 | 107 | 42.799 | 10.24 |
| 346 | 570 | 94.012 | 7.827 |  | 395 | 248 | 60.698 | 9.027 |
| 347 | 43 | 22.071 | 11.555 |  | 396 | 53 | 26.657 | 11.254 |
| 348 | 55 | 27.142 | 11.2 |  | 397 | 198 | 53.113 | 9.352 |
| 349 | 888 | 140.74 | 7.187 |  | 398 | 280 | 67.042 | 8.852 |
| 350 | 200 | 60.941 | 9.338 |  | 399 | 21 | 13.657 | 12.589 |
| 351 | 149 | 45.042 | 9.762 |  | 400 | 421 | 94.255 | 8.264 |
| 352 | 208 | 64.012 | 9.281 |  | 401 | 340 | 74.527 | 8.572 |
| 353 | 1463 | 164.569 | 6.467 |  | 402 | 897 | 130.255 | 7.173 |
| 354 | 187 | 68.698 | 9.435 |  | 403 | 152 | 52.213 | 9.734 |
| 355 | 789 | 106.154 | 7.358 |  | 404 | 620 | 91.669 | 7.705 |
| 356 | 8 | 7.243 | 13.982 |  | 405 | 66 | 36.799 | 10.937 |
| 357 | 710 | 106.983 | 7.51 |  | 406 | 45 | 26.971 | 11.49 |
| 358 | 149 | 44.456 | 9.762 |  | 407 | 785 | 101.326 | 7.365 |
| 359 | 365 | 74.012 | 8.47 |  | 408 | 558 | 103.083 | 7.857 |
| 360 | 721 | 105.912 | 7.488 |  | 409 | 916 | 146.125 | 7.142 |
| 361 | 187 | 70.77 | 9.435 |  | 410 | 376 | 93.326 | 8.427 |
| 362 | 548 | 103.397 | 7.884 |  | 411 | 58 | 31.971 | 11.124 |
| 363 | 553 | 115.64 | 7.87 |  | 412 | 2551 | 231.054 | 5.665 |
| 364 | 156 | 49.042 | 9.696 |  | 413 | 172 | 54.698 | 9.555 |
| 365 | 389 | 78.698 | 8.378 |  | 414 | 815 | 128.296 | 7.311 |
| 366 | 169 | 48.142 | 9.581 |  | 415 | 44 | 25.142 | 11.522 |
| 367 | 168 | 46.284 | 9.589 |  | 416 | 1166 | 155.024 | 6.794 |
| 368 | 422 | 92.154 | 8.26 |  | 417 | 149 | 51.213 | 9.762 |
| 369 | 482 | 96.497 | 8.069 |  | 418 | 1036 | 164.811 | 6.965 |
| 370 | 1925 | 196.61 | 6.071 |  | 419 | 124 | 44.799 | 10.027 |
| 371 | 26 | 17.071 | 12.281 |  | 420 | 700 | 114.397 | 7.53 |
| 372 | 50 | 24.314 | 11.338 |  | 421 | 226 | 63.355 | 9.161 |
| 373 | 232 | 67.912 | 9.124 |  | 422 | 180 | 64.87 | 9.49 |
| 374 | 275 | 65.87 | 8.878 |  | 423 | 446 | 79.426 | 8.181 |
| 375 | 1973 | 187.024 | 6.035 |  | 424 | 360 | 68.284 | 8.49 |
| 376 | 376 | 73.669 | 8.427 |  | 425 | 14 | 10.414 | 13.174 |
| 377 | 60 | 30.142 | 11.075 |  | 426 | 1252 | 173.267 | 6.692 |
| 378 | 228 | 57.698 | 9.149 |  | 427 | 90 | 36.971 | 10.49 |
| 379 | 100 | 39.385 | 10.338 |  | 428 | 564 | 103.154 | 7.842 |
| 380 | 611 | 116.539 | 7.727 |  | 429 | 518 | 100.74 | 7.965 |
| 381 | 418 | 80.355 | 8.274 |  | 430 | 251 | 64.799 | 9.01 |
| 382 | 816 | 113.326 | 7.309 |  | 431 | 263 | 64.698 | 8.943 |
| 383 | 1075 | 157.368 | 6.911 |  | 432 | 440 | 92.669 | 8.2 |
| 384 | 48 | 23.485 | 11.397 |  | 433 | 357 | 76.941 | 8.502 |
| 385 | 386 | 82.669 | 8.389 |  | 434 | 493 | 91.225 | 8.036 |
| 386 | 447 | 79.77 | 8.177 |  | 435 | 164 | 50.456 | 9.624 |
| 387 | 24 | 15.243 | 12.397 |  | 436 | 573 | 103.326 | 7.819 |
| 388 | 556 | 90.598 | 7.863 |  | 437 | 396 | 85.154 | 8.352 |
| 389 | 119 | 41.385 | 10.087 |  | 438 | 158 | 45.385 | 9.678 |
| 390 | 1032 | 146.983 | 6.97 |  | 439 | 815 | 114.64 | 7.311 |
| 391 | 364 | 74.698 | 8.474 |  | 440 | 437 | 82.326 | 8.21 |
| 392 | 119 | 45.213 | 10.087 |  | 441 | 384 | 73.527 | 8.397 |

| No. | Area | Length | ASTM G |  | No. | Area | Length | ASTM G |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 442 | 250 | 66.841 | 9.016 |  | 491 | 40 | 22.657 | 11.66 |
| 443 | 678 | 101.569 | 7.576 |  | 492 | 894 | 130.083 | 7.177 |
| 444 | 39 | 21.485 | 11.696 |  | 493 | 534 | 98.012 | 7.921 |
| 445 | 649 | 101.527 | 7.639 |  | 494 | 23 | 14.243 | 12.458 |
| 446 | 627 | 101.154 | 7.689 |  | 495 | 147 | 45.385 | 9.782 |
| 447 | 1089 | 163.953 | 6.893 |  | 496 | 119 | 48.213 | 10.087 |
| 448 | 756 | 122.468 | 7.419 |  | 497 | 54 | 27.142 | 11.227 |
| 449 | 411 | 79.941 | 8.299 |  | 498 | 87 | 35.142 | 10.539 |
| 450 | 523 | 84.841 | 7.951 |  | 499 | 637 | 122.698 | 7.666 |
| 451 | 280 | 61.284 | 8.852 |  | 500 | 187 | 60.184 | 9.435 |
| 452 | 422 | 80.355 | 8.26 |  | 501 | 756 | 116.012 | 7.419 |
| 453 | 50 | 30.799 | 11.338 |  | 502 | 177 | 47.627 | 9.514 |
| 454 | 623 | 112.054 | 7.698 |  | 503 | 140 | 48.799 | 9.852 |
| 455 | 1050 | 134.397 | 6.945 |  | 504 | 335 | 95.527 | 8.594 |
| 456 | 366 | 72.012 | 8.466 |  | 505 | 217 | 70.113 | 9.22 |
| 457 | 100 | 39.799 | 10.338 |  | 506 | 583 | 100.941 | 7.794 |
| 458 | 347 | 73.426 | 8.543 |  | 507 | 376 | 77.728 | 8.427 |
| 459 | 1458 | 158.125 | 6.472 |  | 508 | 213 | 64.527 | 9.247 |
| 460 | 37 | 20.657 | 11.772 |  | 509 | 15 | 10.657 | 13.075 |
| 461 | 641 | 117.64 | 7.657 |  | 510 | 36 | 29.385 | 11.812 |
| 462 | 321 | 84.912 | 8.655 |  | 511 | 342 | 74.385 | 8.564 |
| 463 | 30 | 19.899 | 12.075 |  | 512 | 310 | 72.042 | 8.705 |
| 464 | 1507 | 198.095 | 6.424 |  | 513 | 503 | 101.527 | 8.007 |
| 465 | 434 | 109.083 | 8.22 |  | 514 | 632 | 102.598 | 7.678 |
| 466 | 548 | 87.426 | 7.884 |  | 515 | 187 | 59.698 | 9.435 |
| 467 | 1911 | 207.853 | 6.081 |  | 516 | 406 | 86.355 | 8.316 |
| 468 | 261 | 62.113 | 8.954 |  | 517 | 307 | 89.255 | 8.719 |
| 469 | 26 | 17.728 | 12.281 |  | 518 | 323 | 83.527 | 8.646 |
| 470 | 227 | 61.87 | 9.155 |  | 519 | 388 | 80.456 | 8.382 |
| 471 | 982 | 137.225 | 7.042 |  | 520 | 291 | 73.627 | 8.797 |
| 472 | 244 | 65.355 | 9.051 |  | 521 | 42 | 28.485 | 11.589 |
| 473 | 911 | 120.64 | 7.15 |  | 522 | 123 | 43.556 | 10.039 |
| 474 | 645 | 126.711 | 7.648 |  | 523 | 73 | 33.728 | 10.792 |
| 475 | 366 | 73.426 | 8.466 |  | 524 | 135 | 45.556 | 9.905 |
| 476 | 271 | 64.355 | 8.899 |  | 525 | 77 | 31.485 | 10.715 |
| 477 | 1092 | 129.196 | 6.889 |  | 526 | 38 | 19.828 | 11.734 |
| 478 | 240 | 60.113 | 9.075 |  | 527 | 57 | 31.314 | 11.149 |
| 479 | 498 | 83.426 | 8.022 |  | 491 | 40 | 22.657 | 11.66 |
| 480 | 524 | 102.012 | 7.948 |  | 492 | 894 | 130.083 | 7.177 |
| 481 | 1767 | 211.539 | 6.194 |  | 493 | 534 | 98.012 | 7.921 |
| 482 | 21 | 22.899 | 12.589 |  | 494 | 23 | 14.243 | 12.458 |
| 483 | 1559 | 167.669 | 6.375 |  | 495 | 147 | 45.385 | 9.782 |
| 484 | 281 | 75.426 | 8.847 |  | 496 | 119 | 48.213 | 10.087 |
| 485 | 196 | 54.284 | 9.367 |  | 497 | 54 | 27.142 | 11.227 |
| 486 | 44 | 23.899 | 11.522 |  | 498 | 87 | 35.142 | 10.539 |
| 487 | 121 | 46.213 | 10.063 |  | 499 | 637 | 122.698 | 7.666 |
| 488 | 409 | 73.669 | 8.306 |  | 500 | 187 | 60.184 | 9.435 |
| 489 | 454 | 101.77 | 8.155 |  | 501 | 756 | 116.012 | 7.419 |
| 490 | 85 | 37.142 | 10.572 |  | 502 | 177 | 47.627 | 9.514 |

| No. | Area | Length | ASTM G |  | No. | Area | Length | ASTM G |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 503 | 140 | 48.799 | 9.852 |  | 516 | 406 | 86.355 | 8.316 |
| 504 | 335 | 95.527 | 8.594 |  | 517 | 307 | 89.255 | 8.719 |
| 505 | 217 | 70.113 | 9.22 |  | 518 | 323 | 83.527 | 8.646 |
| 506 | 583 | 100.941 | 7.794 |  | 519 | 388 | 80.456 | 8.382 |
| 507 | 376 | 77.728 | 8.427 |  | 520 | 291 | 73.627 | 8.797 |
| 508 | 213 | 64.527 | 9.247 |  | 521 | 42 | 28.485 | 11.589 |
| 509 | 15 | 10.657 | 13.075 |  | 522 | 123 | 43.556 | 10.039 |
| 510 | 36 | 29.385 | 11.812 |  | 523 | 73 | 33.728 | 10.792 |
| 511 | 342 | 74.385 | 8.564 |  | 524 | 135 | 45.556 | 9.905 |
| 512 | 310 | 72.042 | 8.705 |  | 525 | 77 | 31.485 | 10.715 |
| 513 | 503 | 101.527 | 8.007 |  | 526 | 38 | 19.828 | 11.734 |
| 514 | 632 | 102.598 | 7.678 |  | 527 | 57 | 31.314 | 11.149 |
| 515 | 187 | 59.698 | 9.435 |  |  |  |  |  |

Average ASTM grain size number (G) is found to 10.86.

4.14 Graphite analysis of sample microstructure after heat treatment

Figure 4.25 Graphite analysis of sample microstructure after heat treatment

Analyzed table

| No. | Area | Class | Circular |
| --- | --- | --- | --- |
| 1 | 7.84 | 5 | 0.14 |
| 2 | 10.98 | 4 | 0.16 |
| 3 | 18.19 | 3 | 0.14 |
| 4 | 4.08 | 6 | 0.21 |
| 5 | 13.17 | 4 | 0.69 |
| 6 | 20.38 | 3 | 0.09 |
| 7 | 3.45 | 6 | 0.52 |
| 8 | 15.68 | 4 | 0.39 |
| 9 | 6.27 | 5 | 0.54 |
| 10 | 59.27 | 2 | 0.46 |
| 11 | 1573.33 | 0 | 0.01 |
| 12 | 53 | 2 | 0.76 |
| 13 | 14.43 | 4 | 0.47 |
| 14 | 28.22 | 3 | 0.7 |
| 15 | 3.76 | 6 | 0.57 |
| 16 | 21.64 | 3 | 0.71 |
| 17 | 42.96 | 2 | 0.77 |
| 18 | 16.93 | 4 | 0.89 |
| 19 | 3.14 | 6 | 0.48 |
| 20 | 4.39 | 6 | 0.67 |
| 21 | 4.08 | 6 | 0.62 |
| 22 | 26.97 | 3 | 0.89 |
| 23 | 27.28 | 3 | 0.39 |
| 24 | 6.59 | 5 | 0.57 |
| 25 | 17.25 | 3 | 0.57 |
| 26 | 5.64 | 5 | 0.49 |
| 27 | 18.82 | 3 | 0.62 |
| 28 | 42.02 | 2 | 0.76 |
| 29 | 79.03 | 1 | 0.44 |
| 30 | 21.01 | 3 | 0.69 |
| 31 | 4.08 | 6 | 0.35 |
| 32 | 7.21 | 5 | 0.62 |
| 33 | 12.23 | 4 | 0.64 |
| 34 | 6.59 | 5 | 1 |
| 35 | 15.05 | 4 | 0.79 |
| 36 | 35.75 | 2 | 0.64 |
| 37 | 85.93 | 1 | 0.56 |
| 36 | 41.71 | 2 | 0.75 |
| 39 | 14.11 | 4 | 0.74 |
| 40 | 27.6 | 3 | 0.68 |
| 41 | 10.35 | 4 | 0.89 |
| 42 | 15.37 | 4 | 0.8 |
| 43 | 24.46 | 3 | 0.8 |
| 44 | 6.9 | 5 | 0.59 |
| 45 | 23.21 | 3 | 0.76 |
| 46 | 31.36 | 3 | 0.56 |
| 47 | 123.56 | 1 | 0.47 |
| 48 | 4.39 | 6 | 0.67 |
| 49 | 123.24 | 1 | 0.8 |
| 50 | 8.78 | 5 | 0.76 |
| 51 | 7.53 | 5 | 0.65 |
| 52 | 10.35 | 4 | 0.89 |
| 53 | 50.18 | 2 | 0.58 |
| 54 | 8.15 | 5 | 0.43 |
| 55 | 3.76 | 6 | 0.57 |
| 56 | 23.52 | 3 | 0.58 |
| 57 | 18.19 | 3 | 0.6 |
| 58 | 11.6 | 4 | 0.38 |
| 59 | 14.11 | 4 | 0.74 |
| 60 | 5.02 | 5 | 0.43 |
| 61 | 8.15 | 5 | 0.7 |
| 62 | 24.77 | 3 | 0.81 |
| 63 | 116.66 | 1 | 0.65 |
| 64 | 17.88 | 3 | 0.93 |
| 65 | 32.3 | 3 | 0.58 |
| 66 | 14.74 | 4 | 0.77 |
| 67 | 36.69 | 2 | 0.66 |
| 68 | 18.5 | 3 | 0.97 |
| 69 | 12.86 | 4 | 0.67 |
| 70 | 24.46 | 3 | 0.35 |
| 71 | 8.47 | 5 | 0.73 |
| 72 | 23.83 | 3 | 0.59 |
| 73 | 3.45 | 6 | 0.52 |
| 74 | 5.02 | 5 | 0.76 |
| 75 | 25.09 | 3 | 0.82 |
| 76 | 103.17 | 1 | 0.94 |
| 77 | 8.15 | 5 | 0.7 |
| 78 | 10.98 | 4 | 0.95 |
| 79 | 11.6 | 4 | 1 |
| 80 | 21.01 | 3 | 0.69 |
| 81 | 24.15 | 3 | 0.6 |

Figure4.26 Grain size distribution

Statistics for nodularity

| No | Content | Data |
| --- | --- | --- |
| 1 | Field Area | 87229.09 sqr um |
| 2 | Nodules per sqr mm | 5548.608 |
| 3 | Nodularity-Count | 86.27% |
| 4 | Nodularity-Area | 79.11% |

4.15 Phase analysis of sample after heat treatment

Iteration 1 for % phase count

Figure 4.27 Phase analysis of sample after heat treatment

Phase data

| Type of Phase | Analyzed Surface (%) |
| --- | --- |
| Graphite | 27.43 |
| Pearlite | 44.2 |
| Ferrite | 21.48 |
| Carbide | 0.08 |
| Other | 6.81 |

Iteration 2 for % phase count

Figure 4.28 Iteration 2 for % phase count

Phase data

| Type of Phase | Analyzed Surface (%) |
| --- | --- |
| Graphite | 26.57 |
| Pearlite | 44.48 |
| Ferrite | 28.89 |
| Carbide | 0 |
| Other | 0.06 |

CHAPTER 5

Conclusion and scope of future work

5.1 Conclusion

The heat treatment on the samples was performed and changes in matrix contents was studied for predicting the mechanical properties of sample through matrix’s constituents like pearlite, carbide etc. This whole study was done on the basis of capturing microstructures and analyzing all by digital image technique.

After capturing the image through GAIA 5.3 software and analyzing, matrix is found ferritic, this contained pearlite, carbide, ferrite & graphite to 34.81%, 40.45%, 14.23%, 10.22%, respectively before normalizing the sample.

After normalizing the sample the percentage of pearlite, carbide and ferrite graphite are found to 44.20, 0.08, 21.48, 27.43.

The change in percentage of Nodularity is found from 92.96(before heat treatment) to 85.61(after heat treatment).

The change in ASTM grain size number is found 8.925(before heat treatment) to 10.86(after heat treatment).

Since Pearlitic content is increased, carbide content decreased and ASTM grain size is found decreased, it can be concluded from here that material has been refined in grain size so its hardness should be increased, ductility should be increased.

The hardness of Si Mo iron sample has been found increased and it has been verified after tested by Brinell Hardness number, after normalizing the sample it comes out to 240 BHN while it was 205 BHN before.

The tensile strength is found to increase from 450 MPa to 550 MPa before and after normalizing the specimen respectively.

The percentage elongation is found to decrease from 12% to 6% before and after normalizing the specimen respectively.

These predictions are correct by verifying the results from image analysis technique with testing of sample with true value of these properties.

5.2 Scope of future work

The cooling rates during heat treatment may be optimized for having better combination of mechanical properties through analyzing changes occurred in microstructure of Si Mo Spheroidal cast iron by image analysis which gives the results quickly.

The effect of molybdenum can be analyzed on Si Mo S.G. Iron for getting its better combination of mechanical properties for material which is operated under high temperature condition through image analysis technique.

Different types of heat treatments can be performed viz. annealing, austempering, hardening etc.& microstructure of Si Mo S.G. iron may be analyzed.

CHAPTER 6

References

- Ductile iron data of sections 2, 3, 4,5,6,7 provided by ductile iron society, America.

- J.C. Margerie,1975,The Notion of Heredity in Cast Iron Metallurgy. The Metallurgy of Cast Iron, Georgi Publishing Co., Saphorin, pp. 545-558.

- ASM Metals Handbook, vol 1, tenth edition, 1990, pp. 6.

- T.Skaland, 1992, A model for graphite formation in ductile iron. PhD – Thesis: page no. 33-34, The Norwegian Institute of Technology, Norway.

- R.E. Smallman, I.R. Harris and M.A. Duggan, 1997 “Microstructure and Material Processing”, vol 63, page 18-29.

- Svein Oddvar Olsen, Torbjørn Skaland,1998, “Inoculation gray and ductile iron a comparison of nucleation sites,  Elkem ASA, Foundry Products Division,Norway.

- Chen, C.Wang, 1998 “Inoculation mechanism of rare earth Mg alloy in molten cast iron”, journal of material science vol 33,page 985-988.

- M. Perzyk, 2001 A.W. Kochanski, Prediction of ductile cast iron quality by artificial neural networks, J. Mater. Process. Techno. 109page 305–330.

- J. Li, L. Lu, M.O. Lai,2001, Quantitative analysis of the irregularity of graphite nodules in cast iron, Mater. Charact. Vol 45, 83–88.

- C.M.Ecob Service, 2003, A Review of Common Metallurgical Defects in Ductile Cast Iron, Elkem AS, Foundry Products Division.

- Vitali Milekhine,2003 “Microstructure of FeSiMg-based Alloys and Mechanical Properties of the Pure FeSi, FeSi2 andMg2Si Phases,Ph.d. theses Norwegian University of Science and Technology (NTNU).

- G.M. Goodrich, Bodycote Tausig, Inc.Skokie, Illinois 2003 “Cast Iron Microstructure Anomalies and Their Causes”, Cast Iron Quality Control Committee 5J Report by American foundry Society.

- Mahmoud Hafiz, 2003, “Mechanical properties of S.g. iron subjected to variable and austempering temperature heat treatment”, vol A340, page no 1-7.

- Robert O'Rourke, 2004, Ductile Iron Society Meeting - South Bend, America, available online at www.ductile.org .

- Jania M. Radzikowska, 2004,”Effect of specimen preparation on evolution of cast iron microstructures”, Foundry research institute, Zakopianska, vol 54, page 287-304.

- B. I. Imasogie and U.Wendt,2004 “Characterization of Graphite Particle Shape In Spheroidal  Graphite Iron Using A Computer-Based Image Analyzer” Journal of Minerals &materials Characterization & Engineering, Vol. 3, No.1, pp 1-12.

- A. Scozzafava, L. Tomesani, A. Zucchelli, 2004, “Image analysis automation of Spheroidal cast iron”, vol 153-154, page 853-859.

- Gustaf O. stberg, 2006 “Perspectives on research on the formation of nodular graphite in cast iron” journal of material and design, vol no.27 pages 1007–1015.

- DI Techniques. SORELMETAL – Suggestions for Ductile Iron Production. Published by RIO TINTO IRON & TITANIUM Inc., Canada.

- www.ductile.org

- www.foundry.elkem.com

- www.mid-atlanticsernices.com

- www.sciencedirect.com

- www.springerlink.com

- www.mse.mtu.edu/casting.

- www.thdick.co.uk/ductile.htm

- www.Specialtycastings.com

# Text boxes

Grain analysis table

Number of Nodular Graphite Particles

%of Nodularity=

Number of Graphite Particles

Pressursed cope runner

Reaction chamber containing

Nodulazer

Sprue post

Pouring basin

Cope runner choke

Example of in-mould process

Low sulphur iron

Alloy divided bar

Lifting cover design

Stops to control cover lift movement

Lifting lug to lift the ladle

Lifting lug to lift tundish cover

Lifting cover for dross removal

Pouring spout

Fill spout

Double tea pot type tundish ladle.

Mg-Fe-Si alloy

Alloy addition: deslagging cover (after metal pour off)

Tea pot type tundish ladle

Iron

Additions and pour out spout

Iron filling

Modified tea pot-spout tundish design

Tea pot tundish ladle

Second generation fixed top tundish ladle

Early fixed tundish cover ladle design

Schematic sketch of original tundish cover ladle

Example of tundish cover ladle design.

Magnesium alloy

Example of sandwich covers ladle design

Cover steel

Step 9-Ductile iron solidifying

Step 8-Casting ductile iron cylinders

Step 6-Obtaining temperature measurement

Step 5-Magnesium treatment in tundish treatment ladle

Step 7-Ductile iron cylinder

Step 2-Taking a chemical analysis sample

Step 4- Preparing to receive molten iron in ductile iron treatment ladle

Step 1-Melting the charge

Step 3-Ready to tap

An example of step by step ductile iron cylinder manufacturing [25]