Analysis of Variation in Parameters and It’s Effects

On

The Quality of Spot Welding

A Dissertation submitted in partial fulfillment

Of the award of Degree of

Master of Engineering

In

Production Engineering

Submitted by

Vikas Dhiman

University Roll No. 12329

Under the Supervision of

Sh. A.K.Madan

Department of Mechanical Engineering

Delhi College of Engineering, Delhi

2009

Certificate

I hereby certify that the work which is being presented in the dissertation entitled “Analysis of Variation in Parameters and Its Effects On  The Quality of Spot Welding”, in partial fulfillment of the requirements for the award of the degree of Master of Engineering in Production and Industrial Engineering, submitted in the Department of Mechanical Engineering, Delhi College of Engineering, Delhi is an authentic record of my own work carried out for a period of one year under the supervision of Prof. A. K. Madan, Professor of Mechanical Engineering Department, Delhi College of Engineering, Delhi.

I have not submitted the matter embodied in this dissertation for the award of any other degree.

Vikas Dhiman

This is to certify that the above statement made by the candidate is true to the best of my knowledge.

Prof. A. K. Madan

Professor

Department of Mechanical & Production Engineering

Delhi College of Engineering,

Delhi-110042 (India)

Acknowledgement

I wish to acknowledge my profound sense of gratitude to my project Guide Sh. A.K. Madan, Mechanical Engineering department Delhi College of Engineering, for his remarkable guidance and many valuable ideas during the preparation of this project. Indeed it was a matter of great felicity and privilege for me to work under his aegis was express my thankfulness to him for his dedicated inspiration, lively interest and patience through my errors with which it would have being impossible to bring the project near completion.

I wish to extend my hearty thanks to all the staff of the department who directly or indirectly helped me in this project work.

And lastly I express sincere gratitude to Prof. S. Maji HoD, Mechanical Engineering Department, Prof. C.K.Dutta, Prof. S.K.Garg, HoD Training and Placement and Production Engineering Department with whose blessing this project was completed.

New Delhi

June-2009

Vikas Dhiman

Mechanical Engineering Department

Delhi College of Engineering

Abstract

Resistance spot welding (RSW) is widely utilized as a joining technique for automobile industry. The purpose of most spot weld qualification procedure is to insure that, for given material, a weld nugget of adequate size can be achieved. There are three recognized parameters of resistance spot welding – weld current, cycle time and forging pressure which affects the nugget size. Due to variation of these parameters, there is also effect on the mechanical properties spot weld joint. The experimental work is done to study the effects of variation of parameters on nugget diameter and properties in resistance spot welding process for a particular isotropic material. The experiments are conducted on isotropic material and its various physical and thermal properties were known. From the fundamental theory of the resistance welding, it is well known that the minimum value of the dynamic resistance (Rmin) and the maximum value of the electrode displacement (Smax) during the welding have relations with the degree of the nugget molten. Therefore, it is assumed that these two parameters may reveal the quality of a welding joint. To verify this assumption, welding tests were carried out to investigate the relationship among the values of Rmin, Smax, and the tensile strength of a molten joint.

Experiments alone cannot easily study the separate effects of many factors involved in the resistance spot welding  process, nor can they accurately predict the complex behaviour of coupled electrical, mechanical and thermal processes during the spot welding procedure. Also the scope is reduced due to excessive time and cost associated with experimental procedures, which involve many influential parameters. FEM is numerical based technique and considered to be powerful tool for solving field problems. In comparison to the analytical analysis, one important merit of this model is that it can be easily applied to a model, which includes the non uniform material properties and/or complex boundaries. Temperature at faying surface (plate to plate interface) attains very high value during the welding process due to application of high value of current. The temperature is not same along the whole dimension but is varying. The present work gives the temperature distribution during the process of resistance spot welding process using computer simulation. The stress distribution taking place in sheet metal due to application of load during the process also presented with help of structural analysis.

Key Words:	spot welding quality, FEM, monitoring, structural analysis, dynamic resistance

CONTENTS

Certificate

Acknowledgement

Abstract

Contents

List of Figures

List of Tables

1. Resistance Spot Welding……………………………………………………………………….1

2.1 Fundamentals of Resistance Spot Welding…………………………………………………2

2.3 Heat Generation…………………………………………………………………………….2

2.4 The Time Factor…………………………………………………………………………….4

2.3 Electrode Tips………………………………………………………………………………5

2.4 Resistance Spot Weld Heat Zones………………………………………………………….6

2.5 Electrode Tip Size……………………………………..……………………………………8

2.6 Pressure or Welding Force………………………………………………………………...10

2.7 Heat Balance………………………………………………………………………………10

2.8 Surface Conditions………………...………………………………………………………11

3. Practical Uses of Resistance Spot Welding…………………………………………………...12

4. Materials Data For Resistance Spot Welding…………………………………………………13

4.1. Mild Steel…………………………………………………………………………………13

4.2 Low Alloy And Medium Carbon Steels…………………………………………………..14

4.3 Stainless Steels…………………………………………………………………………….14

4.4 Steels, Dip Coated or Plated………………………………………………………………15

4.5 Aluminum And Aluminum Alloys………………………………………………………..15

5 Dynamic Resistance……………………………..…………………………………….……..16

5.2 Welding quality estimation………………………..…………………………..………….18

5.3 Electrode Displacement Characteristics………..………………………………………...20

6. Quality of Spot Welding………………………………………………………………………22

6.1 Weld Attributes on Weld Quality/Strength……………………………………………….22

6.2 Quantitative Estimation of a resistance Spot Welding Quality…………………………..26

6.3 The Physical Based Model………………………………………………………………..28

7. About the Spot Weld Machine……..………………………………………………………….35

7.2 Main Technical Data………………………………………………………………………36

7.2 Parameters of IT gun………………………………………………………………………38

7.3 The Micro Hardness Tester…………………………………..……………………………40

7.4 The UTM………………………………………………………………………………….42

7.5 About the FEA tool – ANSYS software…………………………………………………..43

8.  Details of Test Material………………………………………………………………………45

8.2 Experimental Procedure.............................................................................................…...47

8.3 Analytical Procedure……………………………………………………………………...50

8.4 Repeatability………………………………………………......………………………….52

8.5 Limitations of Apparatus…………………………………………………………………53

9 Experimental Results…………………………………………………………………………..54

9.2 The second set of experiments is conducted under following conditions and varying the value of current…………………………………………………………………..………………58

9.3 Analytical Results…………………………………………………………………………63

10. Conclusions…………………………………………………………………………………..74

References………………………………………………………………………………………..76

List of Figures

Fig.1 Spot welding process details…………………………………………………………...……1

Fig.2.1 Resistance and TIG Spot Weld Comparison…………………………………………...…2

Fig. 2.3 Spot Welding Time Cycle……………………………………………………………..…3

Fig. 2.4 Stages in Spot Welds…………………………………………………………..…………4

Fig. 2.5 Resistance Spot Weld Heat Zones………………………………………………..………6

Fig. 2.6 Heat Distribution…………………………………………………………………………7

Fig. 2.7 Techniques For Obtaining Heat Balance………………………………………..………10

Fig.5.1 dynamic resistance……………………………………………………………….………16

Fig. 5.2 Experimental system for MRSW: (a) the photograph, (b) system configuration……….17

Fig. 5.3 Trace of the dynamic resistance in a welding process……………………………..……19

Fig. 5.4 Trace of the electrode…………………………………………………………………...19

Fig.5.6 Photograph of the testing specimen……………………………………………………...21

Fig. 6.1weld’s geometric attributes, as shown in a schematic cross section of a spot weldment..24

Fig. 6.2 A typical electrode displacement pattern………………………………………………..25

Fig. 6.3  RSW sketch and electrical resistance components……………………………………..28

Fig. 6.4 Resistance of the bulk material vs. time………………………………………………...31

Fig. 6.5 RELM vs. time……………………………………………………………………………32

Fig. 6.6 RC vs. time……………………………………………………………………………...34

Fig. 6.8 Electrical resistance R vs. time………………………………………………………….34

7.1 IT Spot Weld Gun……………………………………………………………………………35

Fig 7.2 Display of TE450………………………………………………………………………...37

Fig 7.3 Pyramid shaped diamond for Vickers Hardness Test……………………………………41

Fig. 7.8 Future Tech Micro Hardness tester……………………………………………………..42

Fig 7.9 Universal Testing Machine……………………………………………………………...42

Fig. 8.1 Microstructure of Test Material…………………………………………………………47

Fig 9.1 Time vs. Hardness of Weld Zone(HV)…………………………………………………..55

Fig 9.2 Cycle Time vs. Shear Strength Kgf)……………………………………………………..56

Fig 9.3 Cycle Time vs Hardness of HAZ (HV)………………………………………………….57

Fig 9.4 Cycle Time vs. Nugget Diameter………………………………………………………..57

Fig Cycle fig 9.5 Time vs. Depression…………………………………………………………..58

Fig. 9.6 Current vs, Nugget Diameter……………………………………………………………60

Fig. 9.7 Current vs Hardness of Weld Zone……………………………………………………..60

Fig 9.8 Current vs. Hardness of HAZ……………………………………………………………61

Fig 9.9 Current vs. Shear Strength………………………………………………………………62

Fig 9.10 Microstructure of weld zone……………………………………………………………63

Fig 9.11 Thermal Analysis of spot weld - Meshed Model………………………………………64

Fig 9.10  Temperature distribution at faying surface……………………………………………64

Fig 9.11 Temperature distribution at electrode workpiece interface……………………………65

Fig 9.12 Temperature distribution along the thickness…………………………………….……66

Fig 9.13 Structural Analysis……………………………………………………………………..67

Fig 9.14 Stress Plot at faying surface…………………………………………………………….68

Fig 9.15 Stress Distribution along the thickness…………………………………………...…….69

Fig 9.16 Deformation Plot……………………………………………………………….………70

Fig 9.17 Temperature at faying surface……………………………………………….…………71

Fig 9.18 Stresses at Faying surface………………………………………………………………72

Fig 9.19 Temperature variation at electrode surface………………………………….…………72

List of Tables

Table 5.1 Properties of the stainless steel specimen……………………………………………..18

Table7.1 Specification of the IT Spot Weld Gun………………………………………………..36

Table 7.2 Physical properties of electrode………………………………………………………36

Table 7.3 Types of parameter and their ranges…………………………………………………..38

Table 7.4 hardness testing equipments with specification……………………………………….41

Table 7.5 Specifications of Tensile Testing Machine……………………………………………43

Table 7.6 System Requirements for ANSYS 8.0………………………………………………...44

Table 8.1 Chemical Composition of Test Material………………………………………………45

Table 8.2 Properties of Test Material……………………………………………………………46

Table8.3 Dimensions of Test Piece……………………….……………………………………..47

Table 8.4 Conditions for first experiments………………………………………………………48

Table 8.5 Spots Welds for first experiment………………….…………………………………..48

Table 8.6 Conditions for second experiments.......................................................................…...49

Table 8.7 Spots Welds for second experiment…………...………………………………………49

Table 9.1 Results with variation in Cycle time……………..……………………………………54

Table 9.2 Results with variation in current………………………………………………………59

Table 9.3 Peak to Valley Value………………………………………………………………….62