DECLARATION

I hereby declare that the project entitled “Tribological Analysis of Etched Mild Steel Surface” being submitted by me, is a bona fide record of my own work carried by me under the guidance and supervision of Sh. R.C.SINGH (Assistant Professor) in partial fulfillment of requirements for the award of the Degree of Master of Technology (Production Engineering) in Mechanical Engineering, from Delhi Technological University, Delhi.

The matter embodied in this project has not been submitted for the award of any other degree.

Gaurav  Shukla

Enroll No: DTU/M.tech./106

Roll No    : 05/PRD/2010

CERTIFICATE

This is to certified that the project entitled “Tribological Analysis of Etched Mild Steel Surface” being submitted by Gaurav Shukla (05/prd/2k10), is a bona fide record of his own work carried by him under my guidance and supervision in partial fulfillment of requirements for the award of the Degree of Master of Technology (Production Engineering) in Mechanical Engineering, from Delhi Technological University, Delhi.

The matter embodied in this project has not been submitted in part or full to any other university/institute for the award of any other degree.

R.C.SINGH (Assistant Professor)

DEPT. OF MECH. ENGG.

DELHI TECHNOLOGICAL UNIVERSITY

ACKNOWLEDGEMENT

I have a great pleasure in expressing my deep sense of gratitude and indebtedness to Sh. R.C.SINGH (Assistant Professor) of Mechanical Engineering Department of Delhi Technological University for their continuous guidance and invaluable suggestion and time at all stages from conceptualization to experimental and final completion of this project work. They have guided me for fundamentals and provided many technical papers on the subject matter and thus inculcated the interest and quest for knowledge of this work. He provided constant support and encouragement for successful completion of this work.

I am also grateful to Prof. B.D Pathak Head Department of Mechanical Engineering, for providing the experimental facilities in various labs of the Department.

I also have great respect and indebtedness for Sh. Rajesh Bohra, for his  support and facilities provided for experiments, required for the completion of this special subject.

I am also thankful to all  lab assistants of my college for helping me.

I express my deep felt love and gratitude to my Parents and all nears and dears for giving me great mental support and help whenever I needed.

.

GAURAV SHUKLA

ABSTRACT

The technological age has complex machines used in the industries as well as in daily life. The problem of wear is likely to occur whenever there is relative motion between two mating surfaces resulting the  dimensions of machine component are lost leading and finally failure of components. This causes hazardous effect on surfaces and breakdown of machine. Micro machined smooth and rough parts have high coefficient of friction in elasto hydrodynamic area. It requires micro level of roughness. It contains fluid which reduces friction. Through chemical etching the micro dimples are produced on the components which reduce the metal to metal contact and thus decreasing wear rate .In this research work hexagonal micro dimples have been produced on mild steel disc through chemical etching and subjected to tribological analysis through pin on disc test and found the significant improvement in the wear resistance. Wear test is performed by varying load and velocity of disc. The study shows that the wear rate first decreases and then increases. Coefficient of friction and friction force is determined and appropriate graph is obtained during relative motion between mating surfaces.

CONTENTS

Declaration 											i

Certificate 											ii

Acknowledgement 										iii

Abstract 											iv

List of figures 										viii

List of tables											ix

Abbreviations										x

Chapter 1											1

Introduction											1

1.1      The Consequences of Friction and Wear					2

1.1.A   Friction and wear can decrease national productivity				3

1.1.B    Friction and wear can affect national security					4

1.1.C    Friction and wear can affect quality of life					4

1.1.D 	 Wear causes accident								4

1.2.	Types of wear									7

1.2.A 	Adhesive wear									8

1.2.B 	Abrasive wear									10

1.2.C 	Surface fatigue wear								12

1.2.D  	Fretting wear										13

1.2.E 	 Erosive wear									15

1.3 	 Types of wear test									16

1.3.A  	Scratch test										16

1.3.B  	Slurry Abrasion Test								17

1.3.C  	Friction Test										18

1.3.D 	Air Jet Erosion Test									19

1.3.E	 Pin on Disc Test									19

Chapter 2											21

Literature Review										21

Chapter 3											30

Experimental procedure									30

3.1 	Material										30

3.2 	Sample preparation									32

3.2.A 	Etching										32

3.2.B	 Steps to etch mild steel								34

3.3	 Design of experiment								38

3.4  	Pin on disc test									40

Chapter 4											44

Results and discussions									44

4.1 	Wear rate with mild steel pin in wet condition					44

4.2 	Wear rate with steel pin in dry condition						48

4.3	 Wear rate with brass pin								48

4.4 	Wear rate with brass pin in dry condition						53

Chapter 5											55

Conclusions											55

Chapter 6											57

Future Scope										57

References 											58

Appendix 1											62

Appendix 2											63

Appendix 3											64

Appendix 4	(Reynold equation)								65

LIST OF FIGURES

1.  Abrasive wear of etched mild surface							11

2.  Fretting wear										14

3.  Erosion wear  										15

4.  Slurry abrasion wear									17

5.  Mild steel disc before etching								31

6.  Experimental set up for etching							37

7 . Hexagonal micro holes on disc by etching						38

8.  Wear and friction monitor machine for pin on disc test				40

9.  etched mild disc before wear test							41

10  etched mild disc during wear test							42

11.  pins of brass and mild steel								42

12.  coefficient of friction vs. velocity							45

13.  coefficient of friction vs. load								46

14.  specific wear rate vs. load								47

15. specific wear rate vs. velocity								47

16. coefficient of friction vs. velocity							50

17. coefficient of friction vs. load								51

18. specific wear rate vs. load								52

19. specific wear rate vs. velocity								52

LIST OF TABLES

Table 1. Variables for wear test								39

Table 2.  Specifications of the pin on disk wear and friction monitor			39

Table 3  Variables and result obtained in wet condition with mild steel pin		45

Table 4  Variables and result obtained in dry condition with mild steel pin		48

Table 5  Variables and result obtained in wet condition with brass pin		49

Table 6  Variables and result obtained in dry condition with brass pin		53

ABBREVIATIONS

Symbol 	      		Explanation

µ				co-efficient of friction

Φ				pin diameter

g				grams

Kg 				kilogram

N				load in Newton

Hv				Vickers micro hardness

µm				Micrometer

A˚				Armstrong

d				Intermolecular distance

θ				Angle of incidence

3D				Three dimensional

D1, D2				Diagonals of indenter

Rpm				Revolution per minute

Vw 				 Wear volume

L				Applied load

S				Total sliding distance

K 				Specific wear rate