**SYNTHESIS AND CHARACTERIZATION OF pH SENSITIVE MALEIC ANHYDRIDE AND ACRYLAMIDE HYDROGEL**

Major project-II report submitted for the partial fulfilment for the award of the degree of

**Master of Technology**

In

**Polymer Technology**

Under the supervision of

**Prof D. Kumar**

**Submitted by**

**Mukesh Kumar Mishra**

**(Roll No: 2K13/PTE/11)**



**DEPARTMENT OF APPLIED CHEMISTRY AND POLYMER TECHNOLOGY**

**DELHI TECHNOLOGICAL UNIVERSITY**

***(****FORMERLY DELHI COLLEGE OF ENGINEERING****)***

Delhi - 110042

**CERTIFICATE**

This is to certify that the M.Tech project titled **“SYNTHESIS AND CHARACTERIZATION OF pH SENSITIVE MALEIC ANHYDRIDE AND ACRYLAMIDE HYDROGEL”** which is submitted by Mukesh Kumar Mishra for partial fulfillment of the requirement for the award of the degree of M.Tech in Polymer Technology of Delhi Technological University, Delhi, is a record of the candidate’s own work carried out by him in the Department of Applied Chemistry and Polymer Technology. This report has not been submitted to any other university or institution for the award of any degree or diploma.

 **SIGNATURE OF SUPERVISOR**

**DECLARATION**

I, hereby declare that the major project entitled **“SYNTHESIS AND CHARACTERIZATION OF pH SENSITIVE MALEIC ANHYDRIDE AND ACRYLAMIDE HYDROGEL”** is a record of original work done by me under the guidance of Prof. D. Kumar during the academic session 2014-15.

I also declare that no part of this report has been previously submitted to any university or institution for acquiring any degree or diploma.

MUKESH KUMAR MISHRA

 2K13/PTE/11

**ACKNOWLEDGEMENT**

I wish to express my deep sense of gratitude and veneration to my project guide, **Prof D. Kumar**, Assistant Professor Department of Applied Chemistry and Polymer Technology, Delhi Technological University, Delhi, for her perpetual encouragement, constant guidance, valuable suggestions and continued motivation, which has enabled me to complete this work.

I am deeply indebted to **Prof D. Kumar** Head, department of Applied Chemistry and Polymer Technology, Delhi, Dr. R am Singh, Prof. A.P. Gupta**,** Dr Jai Singh and all faculty members for their constant guidance and facilities to carry out my project work.

I also express my deep sense of gratitude to Ms.ReetuPrabhakar , Research Scholar Department of Applied Chemistry and Polymer Technology for her kind discussion , valuable suggestions and help offered that really made my working in the laboratory so easy and great fun .

I would like to extend my thanks to all the non-teaching staff of the Polymers Technology Department, especially Mr. R.S. Chauhan, Aman, Javed, Siraj, Ankesh&Jeevan Ram of Polymer department.

Thanks to my friends for their contribution.

Mukesh Kumar Mishra

**CONTENTS**

CAPTIONS OF TABLES vi

CAPTIONS OF FIGURES vii

ABSTRACT viii

 **CHAPTER 1: INTRODUCTION 1-11**

* 1. HYDROGEL
	2. TYPES OF HYDROGELS
	3. SYNTHESIS OF HYDROGEL
	4. CROSS LINKING IN HYDROGELS
	5. MONOMERS USED FOR PREPARATION OF HYDROGEL
	6. AIM AND OBJECTIVE

**CHAPTER 2: EXPERIMENTAL 12-14**

2.1 MATERIALS USED

2.2 INSTRUMENTS USED

2.3 SYNTHESIS OF HYDROGEL

2.4 SWELLING TEST

2.5 CHARACTERISATION OF HYDROGEL

**CHAPTER 3: RESULTS AND DISCUSSION 15-26**

* 1. HYDROGEL PREPARATION
	2. SWELLING IN DISTILLED WATER
	3. SWELLING AT DIFFERENT pH
	4. SEM BEHAVIOUR
	5. X RAY DIFFRACTION
	6. FOURIER TRANSFORM INFRARED SPECTROSCOPY

**CHAPTER 4: CONCLUSIONS 26**

**CHAPTER 5: REFERENCES 27-28**

**CAPTIONS OF TABLES**

|  |  |  |
| --- | --- | --- |
|  **Table No.**  |  **TABLE CAPTIONS** | **Page No.** |
| 1.1 | Vinyl monomers used to prepare hydrogels | 9 |
| 3.1 | Molar ratio of maleic anhydride and acrylamide in Hydrogel | 15 |
| 3.2 | Swelling of hydrogel with molar concentration (0.8:1) of maleic anhydride and acrylamide in water | 16 |
| 3.3 | Swelling of hydrogel with molar concentration (0.9:1) of maleic anhydride and acrylamide in water | 18 |
| 3.4 | Swelling of hydrogel with molar concentration (1:1) of maleic anhydride and acrylamide in water | 20 |
| 3.5 | Effect of pH on swelling | 22 |
| 3.6 | Maximum percentage swelling after 24 h at different pH  | 23 |

**CAPTIONS OF FIGURES**

|  |  |  |
| --- | --- | --- |
| **Figure No.** | **Figure** | **Page No.** |
| 3.1 | Percentage swelling of hydrogel of maleic anhydride and acrylamide (0.8:1) M versus time | 17 |
| 3.2 | Percentage swelling of hydrogel of maleic anhydride and acrylamide (0.9:1) M versus time | 19 |
| 3.3 | Percentage swelling of hydrogel of maleic anhydride and acrylamide (1:1) M versus time | 21 |
| 3.4 | Hydrogel of maleic anhydride and acrylamide (1:1) M swelling at different pH | 23 |
| 3.5 | SEM micrograph of hydrogel of maleic anhydride and acrylamide (1:1) M | 24 |
| 3.6 | XRD pattern of hydrogel of maleic anhydride and acrylamide (1 : 1) M | 25 |
| 3.7 | FTIR spectra of hydrogel | 26 |

**ABSTRACT**

Acrylamide/maleic anhydride hydrogels were prepared by using free radical initiator ammonium persulphate. Hydrogels were cross-linked with methylene bisacrylamide. Swelling properties of hydrogels were analysed in distilled water to find out the concentration of acrylamide and maleic anhydride at which swelling is maximum. Maximum swelling of 1310% of hydrogel was obtained at unimolar concentration of acrylamide and maleic anhydride. Also, the maximum swelling of 1450% was reported at pH 8. Surface morphology, crystallinity and structural studies were carried out using scanning electron microscope, X-Ray Diffraction and Fourier Transform Infrared spectroscopy, respectively.